MasterSpec 2014

SECTION 05 31 00

STEEL DECKING

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

GENERAL

RELATED DOCUMENTS

MANDATORY REQUIREMENT:  Retain this article in all Sections of Project Manual.

Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

SUMMARY

Section Includes:

Roof deck.

Composite floor deck.

Noncomposite form deck.

Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

Section 03 30 00 "Cast-in-Place Concrete" for normal-weight and lightweight structural concrete fill over steel deck.

Section 05 12 00 "Structural Steel Framing" for shop- and field-welded shear connectors.

Section 05 50 00 "Metal Fabrications" for framing deck openings with miscellaneous steel shapes.

Section 09 91 13 "Exterior Painting" for repair painting of primed deck and finish painting of deck.

Section 09 91 23 "Interior Painting" for repair painting of primed deck and finish painting of deck.

ACTION SUBMITTALS

Product Data: For each type of deck, accessory, and product indicated.

Shop Drawings:

Include layout and types of deck panels, anchorage details, reinforcing channels, pans, cut deck openings, special jointing, accessories, and attachments to other construction.

INFORMATIONAL SUBMITTALS

Retain "Welding certificates" Paragraph below if retaining "Welding Qualifications" Paragraph in "Quality Assurance" Article.

Welding certificates.

Retain "Product Certificates" Paragraph below to require submittal of product certificates from manufacturers.

Product Certificates: For each type of steel deck.

Retain "Product Test Reports" Paragraph below if required. List other product test reports if required.

Product Test Reports: For tests performed by a qualified testing agency, indicating that each of the following complies with requirements:

Acoustical roof deck.

Evaluation Reports: For steel deck, from ICC-ES.

QUALITY ASSURANCE

AWS states that welding qualifications remain in effect indefinitely unless welding personnel have not welded for more than six months or there is a specific reason to question their ability.

Welding Qualifications: Qualify procedures and personnel according to AWS D1.3, "Structural Welding Code - Sheet Steel."

DELIVERY, STORAGE, AND HANDLING

Protect steel deck from corrosion, deformation, and other damage during delivery, storage, and handling.

Stack steel deck on platforms or pallets and slope to provide drainage. Protect with a waterproof covering and ventilate to avoid condensation.

Retain subparagraph below if acoustical cellular roof deck with insulation is required.

Protect and ventilate acoustical cellular roof deck with factory-installed insulation to maintain insulation free of moisture.

COORDINATION

Retain first paragraph below if project includes acoustical roof deck.

Coordinate installation of sound-absorbing insulation strips in topside ribs of acoustical deck with roofing installation as specified in applicable Roofing Section to ensure protection of insulation strips against damage from effects of weather and other causes.

PRODUCTS

PERFORMANCE REQUIREMENTS

AISI Specifications: Comply with calculated structural characteristics of steel deck according to AISI's "North American Specification for the Design of Cold-Formed Steel Structural Members."

Retain "Fire-Resistance Ratings" Paragraph below only if products specified are part of a fire-resistance-rated assembly. Indicate rating, testing agency, and testing agency's design designation on Drawings.

Fire-Resistance Ratings: Comply with ASTM E 119; testing by a qualified testing agency. Identify products with appropriate markings of applicable testing agency.

Indicate design designations from UL's "Fire Resistance Directory" or from the listings of another qualified testing agency.

ROOF DECK

Retain this article if roof deck is required.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

ASC Profiles, Inc.

Nucor Corp.

Verco Decking, Inc., a Nucor company.

Or Equal.

Roof Deck: Fabricate panels, without top-flange stiffening grooves, to comply with "SDI Specifications and Commentary for Steel Roof Deck," in SDI Publication No. 31, and with the following:

Galvanized-Steel Sheet: ASTM A 653/A 653M, Structural Steel (SS), Grade 33 G60

Deck Profile: As indicated.

Profile Depth: As indicated.

Design Uncoated-Steel Thickness: As indicated.

Design Uncoated-Steel Thicknesses; Deck Unit/Bottom Plate: As indicated.

Span Condition: As indicated.

Side Laps: Interlocking seam.

COMPOSITE FLOOR DECK

Retain this article if composite floor deck is required. Insert minimum section properties here or indicate on Drawings.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

ASC Profiles, Inc.

Nucor Corp.

Verco Decking, Inc., a Nucor company.

Or Equal.

Composite Floor Deck: Fabricate panels, with integrally embossed or raised pattern ribs and interlocking side laps, to comply with "SDI Specifications and Commentary for Composite Steel Floor Deck," in SDI Publication No. 31, with the minimum section properties indicated, and with the following:

Galvanized-Steel Sheet: ASTM A 653/A 653M, Structural Steel (SS), Grade 33, G60 zinc coating.

Profile Depth: As indicated

Retain one steel thickness from "Design Uncoated-Steel Thickness" Subparagraph below or revise to suit Project.

Design Uncoated-Steel Thickness: As indicated.

Span Condition: As indicated.

ACCESSORIES

General: Provide manufacturer's standard accessory materials for deck that comply with requirements indicated.

Side-Lap Fasteners: Corrosion-resistant, hexagonal washer head; self-drilling, carbon-steel screws, No. 10 minimum diameter.

Flexible Closure Strips: Vulcanized, closed-cell, synthetic rubber.

Miscellaneous Sheet Metal Deck Accessories: Steel sheet, minimum yield strength of 33,000 psi, not less than 0.0359-inch design uncoated thickness, of same material and finish as deck; of profile indicated or required for application.

Revise "Pour Stops and Girder Fillers" Paragraph below to suit Project. Pour-stop thickness and profile guidelines are presented in SDI Publication No. 31.

Pour Stops and Girder Fillers: Steel sheet, minimum yield strength of 33,000 psi, of same material and finish as deck, and of thickness and profile indicated Column Closures, End Closures, Z-Closures, and Cover Plates: Steel sheet, of same material, finish, and thickness as deck unless otherwise indicated.

Retain either "Flat Sump Plates" or "Recessed Sump Pans" Paragraph below if required. Recessed sump pans are seldom used. Coordinate with choice of roof drain if recessed sump pans are required.

Flat Sump Plates: Single-piece steel sheet, 0.0747-inch thick, of same material and finish as deck. For drains, cut holes in the field.

Recessed Sump Pans: Single-piece steel sheet, 0.0747-inch thick, of same material and finish as deck, with 3-inch-wide flanges and [level] [sloped] recessed pans of 1-1/2-inch minimum depth. For drains, cut holes in the field.

Shear Connectors:  ASTM A 108, Grades 1010 through 1020 headed stud type, cold-finished carbon steel, AWS D1.1, Type B, with arc shields.

Galvanizing Repair Paint: ASTM A 780 and SSPC-Paint 20 or MIL-P-21035B, with dry film containing a minimum of 94 percent zinc dust by weight.

EXECUTION

EXAMINATION

Examine supporting frame and field conditions for compliance with requirements for installation tolerances and other conditions affecting performance.

Proceed with installation only after unsatisfactory conditions have been corrected.

INSTALLATION, GENERAL

Install deck panels and accessories according to applicable specifications and commentary in SDI Publication No. 31, manufacturer's written instructions, and requirements in this Section.

Install temporary shoring before placing deck panels if required to meet deflection limitations.

Locate deck bundles to prevent overloading of supporting members.

Place deck panels on supporting frame and adjust to final position with ends accurately aligned and bearing on supporting frame before being permanently fastened. Do not stretch or contract side-lap interlocks.

Place deck panels flat and square and fasten to supporting frame without warp or deflection.

Cut and neatly fit deck panels and accessories around openings and other work projecting through or adjacent to deck.

Coordinate reinforcing requirements of openings in first paragraph below with applicable Sections.

Provide additional reinforcement and closure pieces at openings as required for strength, continuity of deck, and support of other work.

Comply with AWS requirements and procedures for manual shielded metal arc welding, appearance and quality of welds, and methods used for correcting welding work.

ROOF-DECK INSTALLATION

This article includes installation requirements for classes of roof deck and form deck used in roof applications. Revise first paragraph below and insert requirements if mechanical fastening to supports is permitted.

Fasten roof-deck panels to steel supporting members by arc spot (puddle) welds of the surface diameter indicated or arc seam welds with an equal perimeter that is not less than 1-1/2 inches long, and as follows:

Retain one weld diameter from "Weld Diameter" Subparagraph below or revise to suit Project.

Weld Diameter: 3/4-inch, nominal.

Weld Spacing: Weld edge and interior ribs of deck units with a minimum of two welds per deck unit at each support. Space welds as indicated. .

Retain "Weld Washers" Subparagraph below if minimum uncoated steel thickness is less than 0.028 inch.

Weld Washers: Install weld washers at each weld location.

SDI requires side-lap and perimeter edge fastening if deck spans exceed 60 inches. Revise fastener spacing in "Side-Lap and Perimeter Edge Fastening" Paragraph below if required.

Side-Lap and Perimeter Edge Fastening: As indicated.

End Bearing: Install deck ends over supporting frame with a minimum end bearing of 1-1/2 inches, with end joints as follows:

End Joints: Lapped 2 inches minimum.

Roof Sump Pans and Sump Plates: Install over openings provided in roof deck and weld flanges to top of deck. Space welds not more than 12 inches apart with at least one weld at each corner.

Install reinforcing channels or zees in ribs to span between supports and weld.

Miscellaneous Roof-Deck Accessories: Install ridge and valley plates, finish strips, end closures, and reinforcing channels according to deck manufacturer's written instructions. Weld to substrate to provide a complete deck installation.

Weld cover plates at changes in direction of roof-deck panels unless otherwise indicated.

Retain "Flexible Closure Strips" Paragraph below if flexible closures are required or permitted. Usually delete if fire-resistance-rated partitions are required.

FLOOR-DECK INSTALLATION

This article includes installation requirements for classes of floor deck and form deck used in floor applications.

Fasten floor-deck panels to steel supporting members by arc spot (puddle) welds of the surface diameter indicated and as follows:

Retain one weld diameter from "Weld Diameter" Subparagraph below or revise to suit Project.

Weld Diameter: 3/4-inch, nominal.

Retain one of two "Weld Spacing" subparagraphs below. First subparagraph is based on SDI specifications. Retain second subparagraph if showing requirements on Drawings.

Weld Spacing: Space and locate welds as indicated.

Retain "Weld Washers" Subparagraph below if minimum uncoated steel thickness is less than 0.028 inch.

SDI requires side-lap and perimeter edge fastening if deck spans exceed 60 inches. Revise fastener spacing in "Side-Lap and Perimeter Edge Fastening" Paragraph below if required.

Side-Lap and Perimeter Edge Fastening: As indicated.

End Bearing: Install deck ends over supporting frame with a minimum end bearing of 1-1/2 inches, with end joints as follows:

End Joints: Butted.

Pour Stops and Girder Fillers: Weld steel sheet pour stops and girder fillers to supporting structure according to SDI recommendations unless otherwise indicated.

Revise "Floor-Deck Closures" Paragraph below to suit Project.

Floor-Deck Closures: Weld steel sheet column closures, cell closures, and Z-closures to deck, according to SDI recommendations, to provide tight-fitting closures at open ends of ribs and sides of deck.

FIELD QUALITY CONTROL

Testing Agency: The District will engage a qualified testing agency to perform tests and inspections.

Remove and replace work that does not comply with specified requirements.

Additional inspecting, at Contractor's expense, will be performed to determine compliance of corrected work with specified requirements.

PROTECTION

Galvanizing Repairs: Prepare and repair damaged galvanized coatings on both surfaces of deck with galvanized repair paint according to ASTM A 780 and manufacturer's written instructions.

Provide final protection and maintain conditions to ensure that steel deck is without damage or deterioration at time of Substantial Completion.

END OF SECTION 05 31 00

Retain this notice in all Sections of Project Manual.

San Diego Unified School District Guide Specifications

Document Version: August 2021