MasterSpec 03/16

SECTION 06 20 23

INTERIOR FINISH CARPENTRY

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

GENERAL

RELATED DOCUMENTS

MANDATORY REQUIREMENT:  Retain this article in all Sections of Project Manual.

Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

SUMMARY

Section Includes:

Revise subparagraphs below to suit Project and to distinguish interior finish carpentry from items made from wood but specified as architectural woodwork.

Interior trim and molding, including non-fire-rated interior door and sidelight frames.

Shelving and clothes rods.

Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

Retain option in first subparagraph below if structural wood is exposed to view.

Section 06 10 53 “Miscellaneous Rough Carpentry” for furring, blocking, and other carpentry work not exposed to view.

Section 09 91 23 "Interior Painting" for priming and backpriming of interior finish carpentry.

ACTION SUBMITTALS

Product Data: For each type of process and factory-fabricated product. Indicate component materials, dimensions, profiles, textures, and colors and include construction and application details.

Include data for wood-preservative treatment from chemical-treatment manufacturer and certification by treating plant that treated materials comply with requirements. Indicate type of preservative used and net amount of preservative retained. Include chemical-treatment manufacturer's written instructions for finishing treated material.

Include data for fire-retardant treatment from chemical-treatment manufacturer and certification by treating plant that treated materials comply with requirements.

For products receiving a waterborne treatment, include statement that moisture content of treated materials was reduced before shipment to Project site to levels specified.

Include copies of warranties from chemical-treatment manufacturers for each type of treatment.

Delete "Samples for Initial Selection" Paragraph below if colors, profiles, and textures are specified or scheduled.

Samples for Initial Selection: For each type of product involving selection of colors, profiles, or textures.

Retain "Samples for Verification" Paragraph below with or without "Samples for Initial Selection" Paragraph above. If retaining below, delete items not needed for control of grain character, color, and finish, or insert other items. Revise if other sizes are required.

Samples for Verification:

For each species and cut of lumber and panel products with non-factory-applied finish, with 1/2 of exposed surface finished, 50 sq. in. for lumber and 8-by-10 inches for panels.

For each finish system and color of lumber and panel products with factory-applied finish, 50 sq. in. for lumber and 8-by-10 inches for panels.

INFORMATIONAL SUBMITTALS

Evaluation Reports: For fire-retardant-treated wood, from ICC-ES.

DELIVERY, STORAGE, AND HANDLING

Stack lumber, plywood, and other panels flat with spacers between each bundle to provide air circulation. Protect materials from weather by covering with waterproof sheeting, securely anchored. Provide for air circulation around stacks and under coverings.

Deliver interior finish carpentry materials only when environmental conditions meet requirements specified for installation areas. If interior finish carpentry materials must be stored in other than installation areas, store only where environmental conditions meet requirements specified for installation areas.

FIELD CONDITIONS

Environmental Limitations: Do not deliver or install interior finish carpentry materials until building is enclosed and weatherproof, wet work in space is completed and nominally dry, and HVAC system is operating and maintaining temperature and relative humidity at occupancy levels during the remainder of the construction period.

Do not install finish carpentry materials that are wet, moisture damaged, or mold damaged.

Indications that materials are wet or moisture damaged include discoloration, sagging, or irregular shape.

Indications that materials are mold damaged include fuzzy or splotchy surface contamination and discoloration.

PRODUCTS

MATERIALS, GENERAL

Lumber: DOC PS 20 and the applicable rules of grading indicated.  If no grading agency is indicated, comply with the applicable rules of any rules-writing agency certified by the American Lumber Standard Committee’s Board of Review.  Grade lumber by an agency certified by the American Lumber Standard Committee’s Board of Review to inspect and grade lumber under the rules indicated.

NHLA: National Hardwood Lumber Association, "Rules for the Measurement and Inspection of Hardwood & Cypress."

RIS:  Redwood Inspection Service.

WCLIB: West Coast Lumber Inspection Bureau, Standard No. 17, "Grading Rules for West Coast Lumber."

WWPA: Western Wood Products Association, "Western Lumber Grading Rules."

Factory mark each piece of lumber with grade stamp of inspection agency indicating grade, species, moisture content at time of surfacing, and mill.

For exposed lumber, mark grade stamp on end or back of each piece.

Softwood Plywood: DOC PS 1.

Hardwood Plywood:  HPVA HP-1.

Each batch shall be accompanied by the appropriate stamp, certifying that the urea formaldehyde emissions are below the voluntary level set by HPMA FE.

WOOD-PRESERVATIVE-TREATED MATERIALS

Category UC1 is suitable for interior dry locations; Category UC2 is suitable for interior damp locations.

Preservative Treatment by Pressure Process: AWPA U1; Use Category UC1.

Maximum moisture contents specified in subparagraph below are standard limits for preservative-treated lumber and plywood that are kiln dried after treatment.

Kiln dry lumber and plywood after treatment to a maximum moisture content of 19 and 18 percent respectively.

Preservative Chemicals: Acceptable to authorities having jurisdiction and containing no arsenic or chromium.

For exposed items indicated to receive transparent finish, do not use chemical formulations that contain colorants or that bleed through or otherwise adversely affect finishes.

Do not use material that is warped or does not comply with requirements for untreated material.

Mark lumber with treatment-quality mark of an inspection agency approved by the American Lumber Standard Committee's Board of Review.

For exposed lumber indicated to receive a stained or natural finish, mark end or back of each piece.

Mark plywood with appropriate classification marking of an inspection agency acceptable to authorities having jurisdiction.

For exposed plywood indicated to receive a stained or natural finish, mark back of each piece.

Application: Where indicated.

FIRE-RETARDANT-TREATED MATERIALS

General: For applications indicated, use materials complying with requirements in this article that are acceptable to authorities having jurisdiction, and comply with testing requirements; testing by a qualified testing agency.

Fire-Retardant-Treated Lumber and Plywood by Pressure Process: Products with a flame-spread index of 25 or less when tested according to ASTM E 84, with no evidence of significant progressive combustion when the test is extended an additional 20 minutes, and with the flame front not extending more than 10.5 feet beyond the centerline of the burners at any time during the test.

Kiln dry lumber and plywood after treatment to a maximum moisture content of 19 and 15 percent respectively.

Delete first paragraph below if no items are to receive a stained or natural finish. Organic resin treatment is more expensive than salt treatments but helps ensure a better stained or natural finish.

For exposed items indicated to receive a stained or natural finish, use organic resin chemical formulations that do not contain colorants, and provide materials that do not have marks from spacer sticks on exposed face.

Do not use material that does not comply with requirements for untreated material or is warped or discolored.

Identify fire-retardant-treated wood with appropriate classification marking of testing and inspecting agency acceptable to authorities having jurisdiction.

For exposed lumber indicated to receive a stained or natural finish, mark end or back of each piece.

For exposed plywood indicated to receive a stained or natural finish, mark back of each piece.

Unless all interior lumber and plywood is required to be fire-retardant treated, insert list of items to be treated in "Application" Paragraph below or indicate on Drawings or in other articles where they are specified.

Application: Where indicated.

INTERIOR TRIM

Softwood Lumber Trim for Transparent Finish (Stain or Clear Finish):

Species and Grade: Douglas fir-larch or Douglas fir south, Superior or C & Btr finish; WCLIB, or WWPA.

Maximum Moisture Content: 19 percent with at least 85 percent of shipment at 12 percent or less.

Finger Jointing: Not allowed.

Face Surface: Surfaced (smooth).

Hardwood Lumber Trim for Transparent Finish (Stain or Clear Finish):

Fourth option in "Species and Grade" Subparagraph below includes light-colored, closed-grain species that will take stain; if retaining, delete undesirable species, if any, from list.

Species and Grade: Clear, kiln-dried white maple, alder, or yellow poplar; NHLA.

Maximum Moisture Content: 9 percent.

Finger Jointing: Not allowed.

Gluing for Width: Not allowed.

Veneered Material: Not allowed.

Face Surface: Surfaced (smooth).

Matching: Selected for compatible grain and color.

Lumber Trim for Opaque Finish (Painted Finish):

Verify local availability before retaining species and grade.

Species and Grade: Idaho white, lodgepole, ponderosa, radiata, or sugar pine; D Select (Quality); WWPA.

Species and Grade: White woods, D Select; WWPA.

Maximum Moisture Content: 15 percent with at least 85 percent of shipment at 12 percent or less.

"Maximum Moisture Content" Subparagraph below is for hardwood boards. NHLA does not define any maximum moisture content values for kiln-dried hardwood lumber; purchaser must specify the value. .

Finger Jointing: Not allowed.

Face Surface: Surfaced (smooth).

Softwood Moldings for Transparent Finish (Stain or Clear Finish): MMPA WM 4, N-grade wood moldings. Made to patterns included in MMPA’s “WM/Series Wood Molding Patterns”.

Species: Douglas fir.

Maximum Moisture Content: 15 percent with at least 85 percent of shipment at 12 percent or less.

Finger Jointing: Not allowed.

Matching: Selected for compatible grain and color.

Hardwood Moldings for Transparent Finish (Stain or Clear Finish): MMPA HWM 4, N-grade wood moldings made to patterns included in MMPA “HWM/Series Hardwood Molding Patterns”.

Third option in "Species" Subparagraph below includes light-colored, closed-grain hardwood species that will take stain; if retaining, delete undesirable species, if any, from list.

Species: Clear, kiln-dried white maple, or yellow poplar.

Maximum Moisture Content: 9 percent.

Finger Jointing: Not allowed.

Matching: Selected for compatible grain and color.

Moldings for Opaque Finish (Painted Finish): Made to patterns included in MMPA “WM/Series Wood Molding Patterns”..

Hardwood Moldings: MMPA HWM 4, P-grade.

Species: Species: Aspen, basswood, cottonwood, gum, magnolia, soft maple, tupelo, or yellow poplar.

Maximum Moisture Content: 9 percent.

Finger Jointing: Not allowed.

Delete below if no wood molding patterns.  Revise if patterns are shown on Drawings or must match existing patterns.

Wood Molding Patterns:  Provide stock moldings made to patterns included in MMPA WM7 and graded under MMPA WM4.

SHELVING AND CLOTHES RODS

Copy "(Exposed) (Closet) (Utility) Shelving" Paragraph below and re-edit as needed to describe different categories of shelving required.

Exposed Utility Shelving: Made from the following material, 3/4 inch thick.

Softwood Boards: Douglas fir-larch, Douglas fir south, or hem-fir; Superior or C & Btr finish; WCLIB, or WWPA; or southern pine, B & B finish; SPIB; kiln dried.

Shelf Cleats: 3/4-by-3-1/2-inch boards, as specified above for.

Shelf Brackets with Rod Support: BHMA A156.16, B04051; prime-painted formed steel.

Shelf Brackets without Rod Support: BHMA A156.16, B04041; prime-painted formed steel.

Standards for Adjustable Shelf Brackets: BHMA A156.9, B04102; powder-coat-finished steel.

Adjustable Shelf Brackets: BHMA A156.9, B04112; powder-coat-finished steel or natural aluminum.

Standards for Adjustable Shelf Supports: BHMA A156.9, B04071; powder-coat-finished steel.

Adjustable Shelf Supports: BHMA A156.9, B04081 or B04091; powder-coat-finished steel.

Clothes Rods: 1-1/2-inch diameter, clear, kiln-dried hardwood.

Clothes Rods (Option to above): 1-5/16-inch-diameter, aluminum tubes, or chromeplated-steel telescoping tubes with end brackets for mounting on shelf cleats.

K. Rod Flanges: Aluminum..

MISCELLANEOUS MATERIALS

Delete materials in this article not required.

Fasteners for Interior Finish Carpentry: Nails, screws, and other anchoring devices of type, size, material, and finish required for application indicated to provide secure attachment, concealed where possible.

Glue: Aliphatic-resin, polyurethane, or resorcinol wood glue recommended by manufacturer for general carpentry use.

Paneling Adhesive: Comply with paneling manufacturer's written recommendations for adhesives.

Multipurpose Construction Adhesive: Formulation complying with ASTM D 3498 that is recommended for indicated use by adhesive manufacturer.

FABRICATION

Back out or kerf backs of the following members except those with ends exposed in finished work:

Interior standing and running trim except shoe and crown molds.

Wood-board paneling.

Ease edges of lumber less than 1-inch in nominal thickness to 1/16-inch radius and edges of lumber 1-inch or more in nominal thickness to 1/8-inch radius.

EXECUTION

EXAMINATION

Examine substrates, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance.

Examine finish carpentry materials before installation. Reject materials that are wet, moisture damaged, and mold damaged.

Proceed with installation only after unsatisfactory conditions have been corrected.

PREPARATION

Clean substrates of projections and substances detrimental to application.

Before installing interior finish carpentry, condition materials to average prevailing humidity in installation areas for a minimum of 24 hours unless longer conditioning is recommended by manufacturer.

INSTALLATION, GENERAL

Do not use materials that are unsound, warped, improperly treated or finished, inadequately seasoned, too small to fabricate with proper jointing arrangements, or with defective surfaces, sizes, or patterns.

Install interior finish carpentry level, plumb, true, and aligned with adjacent materials. Use concealed shims where necessary for alignment.

Scribe and cut interior finish carpentry to fit adjoining work. Refinish and seal cuts as recommended by manufacturer.

Where face fastening is unavoidable, countersink fasteners, fill surface flush, and sand unless otherwise indicated.

Install to tolerance of 1/8-inch in 96 inches for level and plumb. Install adjoining interior finish carpentry with 1/32-inch maximum offset for flush installation and 1/16-inch maximum offset for reveal installation.

Coordinate interior finish carpentry with materials and systems in or adjacent to it. Provide cutouts for mechanical and electrical items that penetrate interior finish carpentry.

STANDING AND RUNNING TRIM INSTALLATION

Install with minimum number of joints practical, using full-length pieces from maximum lengths of lumber available. Do not use pieces less than 24 inches long, except where necessary. Stagger joints in adjacent and related standing and running trim. [Cope] [Miter] at returns, miter at outside corners, and cope at inside corners to produce tight-fitting joints with full-surface contact throughout length of joint. Use scarf joints for end-to-end joints. Plane backs of casings to provide uniform thickness across joints where necessary for alignment.

Match color and grain pattern of trim for transparent finish (stain or clear finish) across joints.

Install trim after gypsum-board joint finishing operations are completed.

Install without splitting; drill pilot holes before fastening where necessary to prevent splitting. Fasten to prevent movement or warping. Countersink fastener heads on exposed carpentry work and fill holes.

SHELVING AND CLOTHES ROD INSTALLATION

Cut shelf cleats at ends of shelves about 1/2-inch less than width of shelves and sand exposed ends smooth.

Install shelf cleats by fastening to framing or backing with finish nails or trim screws, set below face and filled. Space fasteners not more than 16 inches o.c. [ Use 2 fasteners at each framing member or fastener location for cleats 4 inches nominal in width and wider.]

Delete subparagraph below if not required.

Apply a bead of multipurpose construction adhesive to back of shelf cleats before installing. Remove adhesive that is squeezed out after fastening shelf cleats in place.

Install shelf brackets according to manufacturer's written instructions, spaced not more than 32 inches o.c. Fasten to framing members, blocking, or metal backing, or use toggle bolts or hollow wall anchors.

Install standards for adjustable shelf supports according to manufacturer's written instructions. Fasten to framing members, blocking, or metal backing, or use toggle bolts or hollow wall anchors. Space fasteners not more than 12 inches o.c.

Install standards for adjustable shelf brackets according to manufacturer's written instructions, spaced not more than 36 inches o.c. and within 6 inches of end of shelves. Fasten to framing members, blocking, or metal backing, or use toggle bolts or hollow wall anchors.

Cut shelves to neatly fit openings with only enough gap to allow shelves to be removed and reinstalled. Install shelves, fully seated on cleats, brackets, and supports.

Consider deleting first subparagraph below so shelves can be removed for painting.

Fasten shelves to cleats with finish nails or trim screws, set flush.

Usually retain subparagraph below so shelves will provide lateral support for shelf brackets.

Fasten shelves to brackets to comply with bracket manufacturer's written instructions.

Install rod flanges for rods as indicated. Fasten to shelf cleats, framing members, blocking, or metal backing, or use toggle bolts or hollow wall anchors. Install rods in rod flanges.

ADJUSTING

Replace interior finish carpentry that is damaged or does not comply with requirements. Interior finish carpentry may be repaired or refinished if work complies with requirements and shows no evidence of repair or refinishing. Adjust joinery for uniform appearance.

CLEANING

Clean interior finish carpentry on exposed and semiexposed surfaces. Restore damaged or soiled areas and touch up factory-applied finishes, if any.

PROTECTION

Protect installed products from damage from weather and other causes during construction.

Remove and replace finish carpentry materials that are wet, moisture damaged, and mold damaged.

Indications that materials are wet or moisture damaged include discoloration, sagging, or irregular shape.

Indications that materials are mold damaged include fuzzy or splotchy surface contamination and discoloration.

END OF SECTION 06 20 23

Retain this notice in all Sections of Project Manual.

San Diego Unified School District Guide Specifications

Document Version: August 2021