MasterSpec 2014

SECTION 07 62 00

SHEET METAL FLASHING AND TRIM

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

GENERAL

RELATED DOCUMENTS

Retain this article in all Sections of Project Manual.

Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

SUMMARY

Section Includes:

Manufactured reglets with counterflashing.

Formed roof-drainage sheet metal fabrications.

Formed low-slope roof sheet metal fabrications.

Formed wall sheet metal fabrications.

Formed equipment support flashing.

Formed overhead-piping safety pans.

Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.  Add roofing section(s) for roof drain flashing coordination.

Section 06 10 53 "Miscellaneous Rough Carpentry" for wood nailers, curbs, and

blocking.

Section 07 41 13.16 "Standing-Seam Metal Roof Panels" for materials and installation of sheet metal flashing and trim integral with roofing.

Section 07 72 00 "Roof Accessories" for set-on-type curbs, equipment supports, roof hatches, vents, and other manufactured roof accessory units.

COORDINATION

Coordinate sheet metal flashing and trim layout and seams with sizes and locations of penetrations to be flashed, and joints and seams in adjacent materials.

Coordinate sheet metal flashing and trim installation with adjoining roofing and wall materials, joints, and seams to provide leak proof, secure, and noncorrosive installation.

PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

Preinstallation Conference: Conduct conference at Project site.

If needed, insert list of conference participants not mentioned in Section 01 31 00 "Project Management and Coordination."

Retain one or more subparagraphs below if additional agenda items specific to Project are required but not mentioned in Section 01 31 00 "Project Management and Coordination"; revise to suit Project.

Review construction schedule. Verify availability of materials, Installer's personnel, equipment, and facilities needed to make progress and avoid delays.

Review special roof details, roof drainage, roof-penetration flashing, equipment curbs, and condition of other construction that affect sheet metal flashing and trim.

Review sheet metal flashing observation and repair procedures after flashing installation.

ACTION SUBMITTALS

Product Data: For each type of product.

Include construction details, material descriptions, dimensions of individual components and profiles, and finishes for each manufactured product and accessory.

Shop Drawings: For sheet metal flashing and trim.

Include plans, elevations, sections, and attachment details, including attachments to other work.

Detail fabrication and installation layouts, expansion-joint locations, and keyed details. Distinguish between shop- and field-assembled work.

Include identification of material, thickness, weight, and finish for each item and location in Project.

Include details for forming, including profiles, shapes, seams, and dimensions.

Include details for joining, supporting, and securing, including layout and spacing of fasteners, cleats, clips, and other attachments. Include pattern of seams.

Include details of termination points and assemblies.

Include details of expansion joints and expansion-joint covers, including showing direction of expansion and contraction from fixed points.

Include details of roof-penetration flashing.

Include details of edge conditions, including eaves, ridges, valleys, rakes, crickets, and counter flashings as applicable.

Include details of special conditions.

Include details of connections to adjoining work.

Revise subparagraph below to suit Project. Delete if manufacturer's product data are adequate.

Detail formed flashing and trim at scale of not less than 1-1/2 inches per 12 inches.

Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs below for two-stage Samples.

Samples for Initial Selection: For each type of sheet metal and accessory indicated with factory-applied finishes.

Samples for Verification: For each type of exposed finish.

Retain "Sheet Metal Flashing" Subparagraph below if sheet metal flashing and trim are prefinished

Sheet Metal Flashing: 12 inches long by actual width of unit, including finished seam and in required profile. Include fasteners, cleats, clips, closures, and other attachments.

Trim, Metal Closures, Expansion Joints, Joint Intersections, and Miscellaneous Fabrications: 12 inches long and in required profile. Include fasteners and other exposed accessories.

Unit-Type Accessories and Miscellaneous Materials: Full-size Sample.

INFORMATIONAL SUBMITTALS

Coordinate "Qualification Data" Paragraph below with qualification requirements in "Quality Assurance" Article.

Qualification Data: For fabricator.

Product Test Reports: For each product, for tests performed by a qualified testing agency.

Sample Warranty: For special warranty.

CLOSEOUT SUBMITTALS

Maintenance Data: For sheet metal flashing and trim, and its accessories, to include in maintenance manuals.

QUALITY ASSURANCE

Fabricator Qualifications: Employs skilled workers who custom fabricate sheet metal flashing and trim similar to that required for this Project and whose products have a record of successful in-service performance.

Retain “Mockups” paragraph below only for special situations where the added expense is justified.

Mockups: Build mockups to verify selections made under Sample submittals, to demonstrate aesthetic effects, and to set quality standards for fabrication and installation.

Build mockup of typical roof [edge] [eave], including [gutter] [fascia] [fascia trim] [apron flashing] <Insert item>, approximately [10 feet] <Insert dimension> long, including supporting construction cleats, seams, attachments [, underlayment,] and accessories.

Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless District Construction Manager specifically approves such deviations in writing.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 01 40 02 "Quality Requirements / Contractor Laboratory" for demolishing and removing mockups.

Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

DELIVERY, STORAGE, AND HANDLING

Do not store sheet metal flashing and trim materials in contact with other materials that might cause staining, denting, or other surface damage. Store sheet metal flashing and trim materials away from uncured concrete and masonry.

Protect strippable protective covering on sheet metal flashing and trim from exposure to sunlight and high humidity, except to extent necessary for period of sheet metal flashing and trim installation.

WARRANTY

Retain this article only for coil-coated sheet metal. Delete if metal is left uncoated or field finished. Coordinate with finishes retained in Part 2.

Special Warranty on Finishes: Manufacturer agrees to repair finish or replace sheet metal flashing and trim that shows evidence of deterioration of factory-applied finishes within specified warranty period.

Usually retain "Exposed Panel Finish" Subparagraph below for fluoropolymer finish.

Exposed Panel Finish: Deterioration includes:

Color fading more than 5 Hunter units when tested according to ASTM D 2244.

Chalking in excess of a No. 8 rating when tested according to ASTM D 4214.

Cracking, checking, peeling, or failure of paint to adhere to bare metal.

Finish Warranty Period: 20 years from date of Substantial Completion.

PRODUCTS

PERFORMANCE REQUIREMENTS

General: Sheet metal flashing and trim assemblies shall withstand wind loads, structural movement, thermally induced movement, and exposure to weather without failure due to defective manufacture, fabrication, installation, or other defects in construction. Completed sheet metal flashing and trim shall not rattle, leak, or loosen, and shall remain watertight.

Retain first option in "Sheet Metal Standard for Flashing and Trim" Paragraph below for copings and roof edge flashings.  Design copings and roof edge flashings in accordance with NRCA’s certified details to comply with CBC requirements for SPRIES-1 testing.  Retain second option for other flashings.

Sheet Metal Standard for Flashing and Trim: Comply with SMACNA's "Architectural Sheet Metal Manual" requirements for dimensions and profiles shown unless more stringent requirements are indicated.

SPRI Wind Design Standard: Manufacture and install [copings] [roof edge flashings] capable of resisting the following design pressure:

Indicate wind design pressure on Drawings or in "Design Pressure" Subparagraph below. Design pressure is determined by formulas in CBC Chapter 16 that account for basic wind speed, exposure factor, building height, building importance factor, and pressure coefficient that combines a gust factor.

Design Pressure: As indicated on Structural Drawings.

Thermal Movements: Allow for thermal movements from ambient and surface temperature changes to prevent buckling, opening of joints, overstressing of components, failure of joint sealants, failure of connections, and other detrimental effects. Base calculations on surface temperatures of materials due to both solar heat gain and nighttime-sky heat loss.

Temperature Change: 120 deg F, ambient; 180 deg F, material surfaces.

SHEET METALS

Finishes for sheet metals are specified with materials in this article rather than in a separate "Finishes" Article.

General: Protect mechanical and other finishes on exposed surfaces from damage by applying strippable, temporary protective film before shipping.

As a rule, the District does not use stainless steel flashings and trim.  Consider stainless steel for flashings and sheet metal items only for projects located in coastal areas and only after approval by the District Project Manager.  Otherwise, delete stainless steel options.

Stainless-Steel Sheet: ASTM A 240/A 240M Type 316, dead soft, fully annealed; with smooth, flat surface.

Finish: 2D (dull, cold rolled).

Metallic-Coated Steel Sheet: Provide zinc-coated (galvanized) steel sheet according to ASTM A 653/A 653M, G90 coating designation; prepainted by coil-coating process to comply with ASTM A 755/A 755M.

Second option in "Surface" Subparagraph below may diminish oil-canning effect. Retain third option only for field painting galvanized-steel sheet.

Surface: Smooth, flat and mill phosphatized for field painting, if required by coating manufacturer.

Retain "Exposed Coil-Coated Finish" Subparagraph below for factory-coil-coated finish.

Exposed Coil-Coated Finish:

Two-Coat Fluoropolymer: AAMA 621. Fluoropolymer finish containing not less than 70 percent PVDF resin by weight in color coat. Prepare, pretreat, and apply coating to exposed metal surfaces to comply with coating and resin manufacturers' written instructions.

Color: As selected by Architect from manufacturer's full range.

Generally retain "Concealed Finish" Subparagraph below as a factory finish for interior surfaces. For zinc-coated (galvanized) steel sheet, it serves as a protective back coating to protect the zinc from moisture and incompatible substrates.

Concealed Finish: Pretreat with manufacturer's standard white or light-colored acrylic or polyester backer finish, consisting of prime coat and wash coat with minimum total dry film thickness of 0.5-mil.

UNDERLAYMENT MATERIALS

Retain applicable paragraphs in this article for sheet metal flashing and trim applied directly over metal deck, solid sheathing, dissimilar metals, or corrosive substrates. Rosin-sized building paper is used as a slip sheet over other types of underlayment materials.

Felt: ASTM D 226/D 226M, Type II (No. 30), asphalt-saturated organic felt; nonperforated.

Revise Paragraph below if high-temperature underlayment is not required. Slopes are typically limited to not less than 2:12.

Synthetic Underlayment: Laminated or reinforced, woven polyethylene or polypropylene, synthetic roofing underlayment; bitumen free; slip resistant; suitable for high temperatures over 220 deg F; and complying with physical requirements of ASTM D 226/D 226M for Type I and Type II felts.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Atlas Roofing Corporation.

Kirsch Building Products, LLC.

SDP Advanced Polymer Products Inc.

Or Equal.

Underlayment in "Self-Adhering, High-Temperature Sheet" Paragraph below is suitable for higher temperatures associated with exposed sheet metal flashing and trim. Revise if high-temperature underlayment is not required. Slopes are typically limited to not less than 2:12.

Self-Adhering, High-Temperature Sheet: Minimum 30 mils thick, consisting of a slip-resistant polyethylene- or polypropylene-film top surface laminated to a layer of butyl- or SBS-modified asphalt adhesive, with release-paper backing; specifically designed to withstand high metal temperatures beneath metal roofing. Provide primer according to written recommendations of underlayment manufacturer.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Carlisle Coatings & Waterproofing Inc.

Henry Company.

Owens Corning.

Or Equal.

Thermal Stability: ASTM D 1970; stable after testing at 240 deg F or higher.

Low-Temperature Flexibility: ASTM D 1970; passes after testing at minus 20 deg F.or lower.

Retain "Slip Sheet" Paragraph below for separating sheet metal from underlayment. Heavier rosin-sized paper is generally unavailable.

Slip Sheet: Rosin-sized building paper, 3 lb/100 sq. ft. minimum.

MISCELLANEOUS MATERIALS

General: Provide materials and types of fasteners[, solder], protective coatings, sealants, and other miscellaneous items as required for complete sheet metal flashing and trim installation and as recommended by manufacturer of primary sheet metal[ or manufactured item] unless otherwise indicated.

Fasteners: Wood screws, annular threaded nails, self-tapping screws, self-locking rivets and bolts, and other suitable fasteners designed to withstand design loads and recommended by manufacturer of primary sheet metal or manufactured item.

General: Blind fasteners or self-drilling screws, gasketed, with hex-washer head.

Exposed Fasteners: Heads matching color of sheet metal using plastic caps or factory-applied coating. Provide metal-backed EPDM or PVC sealing washers under heads of exposed fasteners bearing on weather side of metal.

Blind Fasteners: High-strength aluminum or stainless-steel rivets suitable for metal being fastened.

Retain applicable fastener subparagraphs below.

Fasteners for Stainless-Steel Sheet: Series 300 stainless-steel.

Fasteners for Zinc-Coated (Galvanized) Steel Sheet: Series 300 stainless steel or hot-dip galvanized steel according to ASTM A 153/A 153M or ASTM F 2329.

Solder:

Retain applicable materials in two subparagraphs below. Soldering requires removal of painted, coated, or lacquered finishes.

For Stainless Steel: ASTM B 32, [Grade Sn60] [Grade Sn96], with acid flux of type recommended by stainless-steel sheet manufacturer.

For Zinc-Coated (Galvanized) Steel: ASTM B 32, with maximum lead content of 0.2 percent.

Sealant Tape: Pressure-sensitive, 100 percent solids, polyisobutylene compound sealant tape with release-paper backing. Provide permanently elastic, nonsag, nontoxic, nonstaining tape 1/2-inch wide and 1/8-inch thick.

Revise "Elastomeric Sealant" Paragraph below if sealant of specific type, grade, class, and use is required.

Elastomeric Sealant: ASTM C 920, elastomeric polyurethane polymer sealant; of type, grade, class, and use classifications required to seal joints in sheet metal flashing and trim and remain watertight.

Bituminous Coating: Cold-applied asphalt emulsion according to ASTM D 1187.

Asphalt Roofing Cement: ASTM D 4586, asbestos free, of consistency required for application.

MANUFACTURED SHEET METAL FLASHING AND TRIM

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Fry Reglet Corporation.

Hickman Company, W. P.

IMETCO

Or equal.

Material: Galvanized steel, 0.028 inch thick.

Retain one or more reglet types and accessories from first five subparagraphs below to suit Project.

Surface-Mounted Type: Provide with slotted holes for fastening to substrate, with neoprene or other suitable weatherproofing washers, and with channel for sealant at top edge.

Stucco Type: Provide with upturned fastening flange and extension leg of length to match thickness of applied finish materials.

Concrete Type: Provide temporary closure tape to keep reglet free of concrete materials, special fasteners for attaching reglet to concrete forms, and guides to ensure alignment of reglet section ends.

Accessories:

Flexible-Flashing Retainer: Provide resilient plastic or rubber accessory to secure flexible flashing in reglet where clearance does not permit use of standard metal counterflashing or where Drawings show reglet without metal counterflashing.

Counterflashing Wind-Restraint Clips: Provide clips to be installed before counterflashing to prevent wind uplift of counterflashing's lower edge.

Finish: With manufacturer's standard factory-applied color coating.

FABRICATION, GENERAL

General: Custom fabricate sheet metal flashing and trim to comply with details shown and recommendations in cited sheet metal standard that apply to design, dimensions, geometry, metal thickness, and other characteristics of item required. Fabricate sheet metal flashing and trim in shop to greatest extent possible.

Fabricate sheet metal flashing and trim in thickness or weight needed to comply with performance requirements, but not less than that specified for each application and metal.

Obtain field measurements for accurate fit before shop fabrication.

Form sheet metal flashing and trim to fit substrates without excessive oil canning, buckling, and tool marks; true to line, levels, and slopes; and with exposed edges folded back to form hems.

Conceal fasteners and expansion provisions where possible. Do not use exposed fasteners on faces exposed to view.

Fabrication Tolerances: Fabricate sheet metal flashing and trim that is capable of installation to a tolerance of 1/4-inch in 20 feet on slope and location lines indicated on Drawings and within 1/8-inch offset of adjoining faces and of alignment of matching profiles.

Expansion Provisions: Form metal for thermal expansion of exposed flashing and trim.

Use lapped expansion joints only where indicated on Drawings.

Sealant Joints: Where movable, nonexpansion-type joints are required, form metal to provide for proper installation of elastomeric sealant according to cited sheet metal standard.

Fabricate cleats and attachment devices from same material as accessory being anchored or from compatible, noncorrosive metal.

Fabricate cleats and attachment devices of sizes as recommended by cited sheet metal standard for application, but not less than thickness of metal being secured.

Retain “Seams” Paragraph below for metals being soldered. Soldering requires removal of painted, coated, or lacquered finishes.

Seams: Fabricate nonmoving seams with flat-lock seams. Tin edges to be seamed, form seams, and solder.

Retain "Seams" Paragraph below for metals with painted, coated, or lacquered finishes.

Seams: Fabricate nonmoving seams with flat-lock seams. Form seams and seal with elastomeric sealant unless otherwise recommended by sealant manufacturer for intended use.

ROOF-DRAINAGE SHEET METAL FABRICATIONS

Retain formed items required in this article. Although the most common fabrications are included, insert descriptions of others if required.

The NRCA and SMACNA recommend minimum size and thicknesses for gutter brackets made from galvanized steel.

Hanging Gutters: Fabricate to cross section required, complete with end pieces, outlet tubes, and other accessories as required. Fabricate in minimum 96-inch-long sections. Furnish flat-stock gutter brackets and flat-stock gutter spacers and straps fabricated from same metal as gutters, of size recommended by cited sheet metal standard but with thickness not less than dimension indicated on Drawings. Fabricate expansion joints, expansion-joint covers, gutter bead reinforcing bars, and gutter accessories from same metal as gutters. Shop fabricate interior and exterior corners.

Detail gutter profiles on Drawings after calculating gutter dimensions to accommodate roof drainage design.  Base gutter profile on SMACNA designations for shapes of formed rectangular hanging gutters.

Gutter Profile: As indicated on Drawings.

Expansion Joints: Lap type.

Accessories: Continuous, removable leaf screen with sheet metal frame and

hardware cloth screen.

Gutters with Girth up to 25 Inches: Fabricate from the following materials:

Galvanized Steel or A-Z alloy-coated steel: 0.034 inch minimum thick.

Gutters with Girth 26 to 30 Inches: Fabricate from the following materials:

Galvanized Steel or A-Z alloy-coated steel: 0.040 inch thick.

Gutters with Girth 31 to 35 Inches: Fabricate from the following material:

Galvanized Steel or A-Z alloy-coated steel: 0.052 inch thick.

Limit use of sheet metal downspouts to areas not subject to vandalism such as from higher roof to lower roof.  Specify downspouts subject to vandalism in Section 22 14 13 “Facility Storm Drainage Piping”.

Downspouts: Fabricate downspouts to dimensions indicated, complete with mitered elbows. Furnish with metal hangers. Shop fabricate elbows.

Hanger Style: As indicated on Drawings.

Fabricate from the following materials:

Galvanized Steel: 0.028-inch thick.

Detail scuppers on Drawings.  Scuppers combined with roof edge flashing (gravel stop) or fascia caps, discharging into hanging gutters or conductor heads, are specified in "Low-Slope Roof Sheet Metal Fabrications" Article.

Parapet Scuppers: Fabricate scuppers to dimensions indicated on Drawings, with closure flange trim to exterior, 4-inch-wide wall flanges to interior, and base extending 4 inches beyond cant or tapered strip into field of roof. Fabricate from the following materials:

Galvanized Steel: 0.028 inch thick.

Conductor Heads: Fabricate conductor heads with flanged back and stiffened top edge and of dimensions and shape indicated on Drawings, complete with outlet tubes, exterior flange trim. Fabricate from the following materials:

Galvanized Steel or A-Z alloy-coated steel: 0.028 inch thick.

Splash Pans: Fabricate to dimensions and shape required and from the following materials:

Galvanized Steel: 0.032 inch thick.

LOW-SLOPE ROOF SHEET METAL FABRICATIONS

Roof Edge Flashing and Fascia Cap: Fabricate in minimum 96-inch-long, but not exceeding 12-foot-long sections. Furnish with 6-inch-wide, joint cover plates. Shop fabricate interior and exterior corners

Joint Style: Butted with expansion space and 6-inch-wide, concealed backup plate.

Fabricate with scuppers spaced 10 feet apart, to dimensions required with 4-inch- wide flanges and base extending 4 inches beyond cant or tapered strip into field of roof. Fasten gravel guard angles to base of scupper.

Fabricate from the Following Materials:

Retain material and thickness of roof edge components that suit wind performance and testing requirements if any.

Galvanized Steel or A-Z alloy-coated steel: 0.028 inch thick.

Copings: Fabricate in minimum 96-inch-long, but not exceeding 12-foot-long, sections. Fabricate joint plates of same thickness as copings. Furnish with continuous cleats to support edge of external leg and drill elongated holes for fasteners on interior leg. Miter corners, fasten and seal or solder or weld watertight. Shop fabricate interior and exterior corners.

Detail coping profile on Drawings.

Coping Profile: As indicated on Drawings.

Options in "Joint Style" Subparagraph below describe joint configurations detailed by SMACNA and the NRCA. Revise to suit Project. Insert descriptions here or show special corner and edge styles on Drawings if required.

Joint Style: Butted with expansion space and 6-inch-wide, concealed backup plate.

Fabricate from the Following Materials:

Galvanized Steel or A-Z alloy-coated steel: 0.040 inch thick.

Roof-to-Wall Transition; Roof-to-Roof Edge-Flashing Transition; Roof-to-Roof Edge-Flashing and Fascia-Cap Transition Expansion-Joint Cover: Fabricate from the following materials: Shop fabricate interior and exterior corners.

Galvanized Steel: 0.034 inch thick.

Counterflashing: Shop fabricate interior and exterior corners. Fabricate from the following materials:

Galvanized Steel: 0.028 inch thick.

Flashing Receivers: Fabricate from the following materials:

Galvanized Steel: 0.028 inch thick.

Roof-Penetration Flashing: Fabricate from the following materials:

Galvanized Steel: 0.028 inch thick.

Roof-Drain Flashing:  Fabricate from stainless steel.

WALL SHEET METAL FABRICATIONS

Retain paragraphs in this article to suit Project. Although the most common fabrications are included, insert descriptions of others if required.

Retain "Opening Flashings in Frame Construction" Paragraph below for nonmasonry-clad wood or cold-formed steel-framed walls. Flashing may be required to surround wall-opening components such as windows, doors, and louvers.

Opening Flashings in Frame Construction: Fabricate head, sill, jamb, and similar flashings to extend 4 inches beyond wall openings. Form head and sill flashing with 2- inch-high, end dams. Fabricate from the following materials:

Galvanized Steel: 0.028 inch thick.

Wall Expansion-Joint Cover: Fabricate from the following materials:

Galvanized Steel: 0.028 inch thick.

MISCELLANEOUS SHEET METAL FABRICATIONS

Retain paragraphs in this article to suit Project. Although the most common fabrications are included, insert descriptions of others if required.

Equipment Support Flashing: Fabricate from the following materials:

Galvanized Steel: 0.028 inch thick.

Overhead-Piping Safety Pans: Fabricate from the following materials:

Galvanized Steel: 0.028 inch thick.

EXECUTION

EXAMINATION

Examine substrates, areas, and conditions, with Installer present, for compliance with requirements for installation tolerances, substrate, and other conditions affecting performance of the Work.

Retain first subparagraph below if retaining requirements for tolerances.

Verify compliance with requirements for installation tolerances of substrates.

Verify that substrate is sound, dry, smooth, clean, sloped for drainage, and securely anchored.

Retain subparagraph below for sheet metal flashing and trim that are part of roof assembly that depends on air- or water-resistant barriers to prevent air infiltration or water penetration and that are located immediately beneath roofing.

Verify that air- or water-resistant barriers have been installed over sheathing or backing substrate to prevent air infiltration or water penetration.

Proceed with installation only after unsatisfactory conditions have been corrected.

UNDERLAYMENT INSTALLATION

Felt Underlayment: Install felt underlayment, wrinkle free, using adhesive to minimize use of mechanical fasteners under sheet metal flashing and trim. Apply in shingle fashion to shed water, with lapped joints of not less than 2 inches.

Synthetic Underlayment: Install synthetic underlayment, wrinkle free, according to manufacturers' written instructions, and using adhesive where possible to minimize use of mechanical fasteners under sheet metal.

Self-Adhering Sheet Underlayment: Install self-adhering sheet underlayment, wrinkle free. Prime substrate if recommended by underlayment manufacturer. Comply with temperature restrictions of underlayment manufacturer for installation; use primer for installing underlayment at low temperatures. Apply in shingle fashion to shed water, with end laps of not less than 6 inches staggered 24 inches between courses. Overlap side edges not less than 3-1/2 inches. Roll laps and edges with roller. Cover underlayment within 14 days.

Retain paragraph below if slip sheet is required. See sheet metal manufacturer's written recommendations.

INSTALLATION, GENERAL

General: Anchor sheet metal flashing and trim and other components of the Work securely in place, with provisions for thermal and structural movement. Use fasteners, solder, protective coatings, separators, sealants, and other miscellaneous items as required to complete sheet metal flashing and trim system.

Install sheet metal flashing and trim true to line, levels, and slopes. Provide uniform, neat seams with minimum exposure of solder, welds, and sealant.

Install sheet metal flashing and trim to fit substrates and to result in watertight performance. Verify shapes and dimensions of surfaces to be covered before fabricating sheet metal.

Space cleats not more than 12 inches apart. Attach each cleat with at least two fasteners. Bend tabs over fasteners.

Install exposed sheet metal flashing and trim with limited oil canning, and free of buckling and tool marks.

Torch cutting of sheet metal flashing and trim is not permitted.

Metal Protection: Where dissimilar metals contact each other, or where metal contacts pressure-treated wood or other corrosive substrates, protect against galvanic action or corrosion by painting contact surfaces with bituminous coating or by other permanent separation as recommended by sheet metal manufacturer or cited sheet metal standard.

Coat concealed side of stainless-steel sheet metal flashing and trim with bituminous coating where flashing and trim contact wood, ferrous metal, or cementitious construction.

Underlayment: Where installing sheet metal flashing and trim directly on cementitious or wood substrates, install underlayment and cover with slip sheet.

Expansion Provisions: Provide for thermal expansion of exposed flashing and trim. Space movement joints at maximum of 10 feet with no joints within 24 inches of corner or intersection.

Revise two subparagraphs below to suit Project.

Form expansion joints of intermeshing hooked flanges, not less than 1 inch deep, filled with sealant concealed within joints.

Use lapped expansion joints only where indicated on Drawings.

Fasteners: Use fastener sizes that penetrate wood blocking or sheathing not less than 1-1/4 inches for nails and not less than 3/4 inch for wood screws.

Conceal fasteners and expansion provisions where possible in exposed work and locate to minimize possibility of leakage. Cover and seal fasteners and anchors as required for a tight installation.

Seal joints as required for watertight construction.

Use sealant-filled joints unless otherwise indicated. Embed hooked flanges of joint members not less than 1-inch into sealant. Form joints to completely conceal sealant. When ambient temperature at time of installation is between 40 and 70 deg F, set joint members for 50 percent movement each way. Adjust setting proportionately for installation at higher ambient temperatures. Do not install sealant-type joints at temperatures below 40 deg F.

Prepare joints and apply sealants to comply with requirements in Section 07 92 00 "Joint Sealants."

Soldered Joints: Clean surfaces to be soldered, removing oils and foreign matter. Pre-tin edges of sheets with solder to width of 1-1/2 inches; however, reduce pre-tinning where pre-tinned surface would show in completed Work.

Do not solder metallic-coated steel sheet.

Do not use torches for soldering.

Heat surfaces to receive solder, and flow solder into joint. Fill joint completely. Completely remove flux and spatter from exposed surfaces.

Stainless-Steel Soldering: Tin edges of uncoated sheets, using solder for stainless steel and acid flux. Promptly remove acid flux residue from metal after tinning and soldering. Comply with solder manufacturer's recommended methods for cleaning and neutralization.

ROOF-DRAINAGE SYSTEM INSTALLATION

General: Install sheet metal roof-drainage items to produce complete roof-drainage system according to cited sheet metal standard unless otherwise indicated. Coordinate installation of roof perimeter flashing with installation of roof-drainage system.

Hanging Gutters: Join sections with with riveted and soldered joints. Provide for thermal expansion. Attach gutters at eave or fascia to firmly anchor them in position. Provide end closures and seal watertight with sealant. Slope to downspouts.

Revise subparagraphs below to suit Project. See "The NRCA Roofing Manual" and SMACNA's "Architectural Sheet Metal Manual" for illustrations of gutters and design recommendations.

Fasten gutter spacers to front and back of gutter.

Anchor and loosely lock back edge of gutter to continuous cleat.

Anchor back of gutter that extends onto roof deck with cleats spaced not more

- than 24 inches apart.

Anchor gutter with gutter brackets spaced not more than 30 inches apart to roof deck, unless otherwise indicated, and loosely lock to front gutter bead.

Install gutter with expansion joints at locations indicated, but not exceeding, 40

- feet apart. Install expansion-joint caps.

Install continuous gutter screens on gutters with noncorrosive fasteners, removable for cleaning gutters.

Downspouts: Join sections with 1-1/2-inch telescoping joints.

Provide hangers with fasteners designed to hold downspouts securely to walls. Locate hangers at top and bottom and at approximately 60 inches o.c.

Provide elbows at base of downspout to direct water away from building.

Retain "Splash Pans" Paragraph below for metal splash pans.

Splash Pans: Install where downspouts discharge on low-slope roofs. Set in elastomeric sealant compatible with the substrate.

Parapet Scuppers: Continuously support scupper, set to correct elevation, and seal flanges to interior wall face, over cants or tapered edge strips, and under roofing membrane.

Retain first subparagraph below if scupper terminates at exterior wall. Retain second subparagraph, with first, if scupper discharges into conductor head set immediately below base elevation of scupper. Retain third subparagraph if scupper discharges directly into back of conductor head.

Anchor scupper closure trim flange to exterior wall and solder or seal with elastomeric sealant to scupper.

Loosely lock front edge of scupper with conductor head.

[Solder] [or] [seal with elastomeric sealant] exterior wall scupper flanges into back of conductor head.

Conductor Heads: Anchor securely to wall, with elevation of conductor head rim at minimum of 1 inch below scupper or gutter discharge.

Expansion-Joint Covers: Install expansion-joint covers at locations and of configuration indicated. Lap joints minimum of 4 inches in direction of water flow.

ROOF FLASHING INSTALLATION

Retain this article for low-slope and steep-slope roof flashing. Coordinate steep-slope roof flashing requirements with applicable steep-slope roofing Section. Revise the Section Text if fastener spacings are detailed on Drawings.

Retain option in "General" Paragraph below if manufactured reglets are required.

General: Install sheet metal flashing and trim to comply with performance requirements, sheet metal manufacturer's written installation instructions, and cited sheet metal standard. Provide concealed fasteners where possible, and set units true to line, levels, and slopes. Install work with laps, joints, and seams that are permanently watertight and weather resistant.

Roof Edge Flashing: Anchor to resist uplift and outward forces according to recommendations in cited sheet metal standard unless otherwise indicated. Interlock bottom edge of roof edge flashing with continuous cleat anchored to substrate at staggered 3-inch centers.

Copings: Anchor to resist uplift and outward forces according to recommendations in cited sheet metal standard unless otherwise indicated.

Interlock exterior bottom edge of coping with continuous cleat anchored to substrate at 24-inch centers.

Anchor interior leg of coping with washers and screw fasteners through slotted holes at 24-inch centers.

Pipe or Post Counterflashing: Install counterflashing umbrella with close-fitting collar with top edge flared for elastomeric sealant, extending minimum of 4 inches over base flashing. Install stainless-steel draw band and tighten.

First two options in "Counterflashing" Paragraph below are based on NRCA and SMACNA recommendations.

Counterflashing: Coordinate installation of counterflashing with installation of base flashing. Insert counterflashing in reglets or receivers and fit tightly to base flashing. Extend counterflashing 4 inches over base flashing. Lap counterflashing joints minimum of 4 inches. Secure in waterproof manner by means of interlocking folded seam or blind rivets and sealant unless otherwise indicated.

Roof-Penetration Flashing: Coordinate installation of roof-penetration flashing with installation of roofing and other items penetrating roof. Seal with elastomeric sealant and clamp flashing to pipes that penetrate roof.

WALL FLASHING INSTALLATION

General: Install sheet metal wall flashing to intercept and exclude penetrating moisture according to cited sheet metal standard unless otherwise indicated. Coordinate installation of wall flashing with installation of wall-opening components such as windows, doors, and louvers.

Opening Flashings in Frame Construction: Install continuous head, sill,[ jamb,] and similar flashings to extend [4 inches] <Insert dimension> beyond wall openings.

MISCELLANEOUS FLASHING INSTALLATION

Equipment Support Flashing: Coordinate installation of equipment support flashing with installation of roofing and equipment. Weld or seal flashing with elastomeric sealant to equipment support member.

Overhead-Piping Safety Pans: Suspend pans from structure above, independent of other overhead items such as equipment, piping, and conduit, unless otherwise indicated on Drawings. Pipe and install drain line to plumbing waste or drainage system.

Insert specific installation requirements here for other sheet metal flashing and trim items specified in this Section if required.

ERECTION TOLERANCES

Installation Tolerances: Shim and align sheet metal flashing and trim within installed tolerance of 1/4 inch in 20 feet on slope and location lines indicated on Drawings and within 1/8-inch offset of adjoining faces and of alignment of matching profiles.

CLEANING AND PROTECTION

Retain first paragraph below for metal surfaces unless metal is painted, coated, or lacquered.

Clean exposed metal surfaces of substances that interfere with uniform oxidation and weathering.

Retain first paragraph below for soldered joints.

Clean and neutralize flux materials. Clean off excess solder.

Clean off excess sealants.

Remove temporary protective coverings and strippable films as sheet metal flashing and trim are installed unless otherwise indicated in manufacturer's written installation instructions. On completion of sheet metal flashing and trim installation, remove unused materials and clean finished surfaces as recommended by sheet metal flashing and trim manufacturer. Maintain sheet metal flashing and trim in clean condition during construction.

Replace sheet metal flashing and trim that have been damaged or that have deteriorated beyond successful repair by finish touchup or similar minor repair procedures.

END OF SECTION 07 62 00

Retain this notice in all Sections of Project Manual.

San Diego Unified School District Guide Specifications

Document Version: August 2021