MasterSpec 2014

SECTION 09 91 23

INTERIOR PAINTING

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

GENERAL

RELATED DOCUMENTS

MANDATORY REQUIREMENT:  Retain this article in all Sections of Project Manual.

Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

SUMMARY

Section includes surface preparation and the application of paint systems on the following interior substrates:

Concrete.

Concrete masonry units (CMUs).

Steel and iron.

Galvanized metal.

Wood.

Gypsum board.

ASJ insulation covering.

Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

Primers in other Sections must be coordinated for compatibility with finish coats specified in this Section. Review other Sections for shop-primed products, and insert references to this Section to establish primer requirements.

Section 05 12 00 "Structural Steel Framing" for shop priming structural steel.

Section 05 50 00 "Metal Fabrications" for shop priming metal fabrications.

Section 09 91 13 “Exterior Painting”.

ACTION SUBMITTALS

Product Data: For each type of product. Include preparation requirements and application instructions.

Samples for Initial Selection:  For each type of topcoat product.

Indicate VOC content.

Delete "Samples for Initial Selection" Paragraph above if colors and other characteristics are preselected and specified or scheduled. Retain "Samples for Verification" Paragraph below with or without above.

Samples for Verification: For each type of paint system and in each color and gloss of topcoat.

Color and gloss of Samples change as they age; seven-day old Samples appear different from freshly dried Samples.

Submit Samples on rigid backing, 8 inches square.

Apply coats on Samples in steps to show each coat required for system.

Label each coat of each Sample.

Label each Sample for location and application area.

Product List: Cross-reference to paint system and locations of application areas. Use same designations indicated on Drawings and in schedules. Include color designations.

QUALITY ASSURANCE

Paint Contractor shall have a minimum of five years documented experience in application of paints and coatings specified.  Contractor shall maintain qualified painting crews during entire painting process.

Regardless of selected paint manufacturer, Contractor is to provide exact color and gloss to match Architect’s selection at no additional cost.

DELIVERY, STORAGE, AND HANDLING

Store materials not in use in tightly covered containers in well-ventilated areas with ambient temperatures continuously maintained at not less than 45 deg F.

Maintain containers in clean condition, free of foreign materials and residue.

Remove rags and waste from storage areas daily.

If necessary, insert special requirements for fire protection, heating, ventilation, and other conditions for storage areas on-site.

FIELD CONDITIONS

Apply paints only when temperature of surfaces to be painted and ambient air temperatures are between 50 and 95 deg F.

Do not apply paints when relative humidity exceeds 85 percent; at temperatures less than 5 deg F above the dew point; or to damp or wet surfaces.

EXTRA MATERIALS

Do not provide any extra materials.

PRODUCTS

MANUFACTURERS

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

PPG Industries.

Sherwin-Williams Company (The).

Vista Paint Corporation.

Dunn-Edwards Paints.

Or Equal.

PAINT, GENERAL

Do not provide materials that contain substances classified by the Global Hazard System as carcinogenic.

Do not provide materials that contain substances listed in the Significant New Use Rule (SNUR) under Toxic Substances Control Act (TSCA)

Material Compatibility:

Systems could fail if paints used for individual coats are incompatible.

Materials for use within each paint system shall be compatible with one another and substrates indicated, under conditions of service and application as demonstrated by manufacturer, based on testing and field experience.

For each coat in a paint system, products shall be recommended in writing by topcoat manufacturers for use in paint system and on substrate indicated.

Colors: As indicated in a color schedule on the Drawings.

Gloss or Sheen Level: As directed by Architect, either on Drawings or by reviewed submittals. Verify this for each item to be painted, prior to commencing painting.

Material Quality:  Provide manufacturer’s best quality paint material of the various types specified that are factory formulated and recommended by manufacturer for application indicated.  Use only paint material containers displaying manufacturer’s product identification.

Regulatory Requirements: Coatings shall comply with the testing and product requirements of San Diego Air Pollution Control District Rule 67.0 "Architectural Coatings."

SOURCE QUALITY CONTROL

Retain this article for large projects or critical coatings where additional control is needed. Delete if tests are not required.

Testing of Paint Materials: District reserves the right to invoke the following procedure:

District will engage the services of a qualified testing agency to sample paint materials. Contractor will be notified in advance and may be present when samples are taken. If paint materials have already been delivered to Project site, samples may be taken at Project site. Samples will be identified, sealed, and certified by testing agency.

Testing agency will perform tests for compliance with product requirements.

District may direct Contractor to stop applying paints if test results show materials being used do not comply with product requirements. Contractor shall remove noncomplying paint materials from Project site, pay for testing, and repaint surfaces painted with rejected materials. Contractor will be required to remove rejected materials from previously painted surfaces if, on repainting with complying materials, the two paints are incompatible.

BLOCK FILLERS

Interior/Exterior Latex Block Filler:

Dunn-Edwards Paints; SBSL00 Smooth Bloc-Fil Select.

Sherwin-Williams Company; B25W25 Block Filler.

Vista Paint Corporation; 40 Block Kote.

Or Equal.

PRIMERS/SEALERS

Interior Latex Primer/Sealer for gypsum board:

Dunn-Edwards Paints; VNSL00 Vinylastic Select.

Sherwin-Williams Company; ProMar 200 Zero VOC Primer, B28W2600.

Vista Paint Corporation; 5000 V-Pro Primer.

Or Equal.

Interior Latex Primer/Sealer for concrete, plaster and porous surfaces:

Dunn-Edwards Paints; UGPR00 Ultra-Grip Premium.

Sherwin-Williams Company; Prep Rite ProBlock B51W8020.

Vista Paint Corporation; 4000 Uniprime.

Or Equal.

Wood-Knot Sealer:  Sealer recommended in writing by topcoat manufacturer for use in paint systems indicated.

METAL PRIMERS

Acrylic Ferrous Metal Primer:

Dunn-Edwards Paints; ENPR00 EnduraPrime.

Sherwin-Williams Company; ProCryl B66.

Vista Paint Corporation; 4800 Metal Primer.

Or Equal.

Acrylic Non-Ferrous Metal Primer:

Dunn-Edwards Paints; ENPR00 EnduaPrime.

Sherwin-Williams Company; ProCryl B66

Vista Paint Corporation; 4800 Metal Pro Acrylic Metal Primer.

Or Equal.

Non-Ferrous Metal Pretreatment:

Dunn-Edwards Paints; Krud Kutter Metal Clean and Etch.

Sherwin-Williams Company; GLL Clean ‘n Etch.

Vista Paint Corporation; Jasco Prep ‘n Prime.

Or Equal.

WOOD PRIMERS

Interior Latex Wood Primer:

Dunn-Edwards Paints; DCPR00 DecoPrime.

Sherwin-Williams Company; Pro Block B51W8020.

Vista Paint Corporation; 4000 Uniprime.

Or Equal.

ACRYLIC LATEX PAINTS

Typically, do not use flat paint.  Consider deleting the following paragraph and retaining paragraph F.

Interior Acrylic Latex (Flat):

Dunn-Edwards Paints; SWLL10 SpartaWall Flat.

Sherwin-Williams Company; ProMar 200 Zero VOC Flat B30W2600.

Vista Paint Corporation; 8100 Carefree.

Or Equal.

Consider deleting the following paragraph and retaining paragraph G.

Interior Acrylic Latex (Eggshell):

Dunn-Edwards Paints; SWLL30 Sparta Wall Eggshell.

Sherwin-Williams Company; ProMar 200 Zero VOC Eggshell B20W2600.

Vista Paint Corporation; 8300 Carefree.

Or Equal.

Interior Acrylic Latex (Low Sheen):

Dunn-Edwards Paints; SWLL40 Sparta Wall Low Sheen.

Sherwin-Williams Company; ProMar 200 Zero VOC Low Sheen, B24-2600.

Vista Paint Corporation; 8200 Carefree Velvasheen

Or Equal.

Interior Acrylic Latex (Semigloss):

Dunn-Edwards Paints; SWLL50 Sparta Wall Semi Gloss.

Sherwin-Williams Company; ProIndustrial DTM Acrylic Semigloss B66-1150.

Vista Paint Corporation; 8400 Carefree.

Or Equal.

Interior Acrylic Latex (Gloss):

Dunn-Edwards Paints; ASHL70 AristoShield.

Sherwin-Williams Company; ProIndustrial DTM Acrylic Gloss B66-1050.

Vista Paint Corporation; 8500 Carefree.

Or Equal.

Institutional Low-Odor/VOC Latex (Flat):

Dunn-Edwards Paints; SWLL10 SpartaWall Flat.

Sherwin-Williams Company; ProMar 200 Zero VOC Flat B30-2600.

Vista Paint Corporation; 5100 V-Pro Flat.

Or Equal.

Institutional Low-Odor/VOC Latex (Eggshell):

Dunn-Edwards Paints; SWLL30 SpartaWall Eggshell.

Sherwin-Williams Company; ProMar 200 Zero VOC Eggshell B20-2600.

Vista Paint Corporation; 5300 V-Pro Eggshell.

Or Equal.

Institutional Low-Odor/VOC Latex (Semigloss):

Dunn-Edwards Paints; SWLL50 SpartaWall Semi Gloss.

Sherwin-Williams Company; ProMar 200 Zero VOC Semigloss B31-2600.

Vista Paint Corporation; 5400 V-Pro Semi-gloss.

Or Equal.

DRY FOG/FALL COATINGS

Latex Dry Fog/Fall:

Dunn-Edwards Paints; AQUA10 AQUAFALL Flat.

Sherwin-Williams Company; Low VOC WB Dryfall Flat B42W81

Vista Paint Corporation; DF12 Dry Fall.

Or Equal.

FLOOR COATINGS

Interior/Exterior Clear Concrete Floor Sealer (Water Based):

Dunn-Edwards Paints; OKN-06 Okon Seal and Finish.

Sherwin-Williams Company; H&C WL Sealer.

Vista Paint Corporation; Monpole Aquaseal SS.

Or Equal.

Latex Floor Enamel (Non-skid, low gloss):

Dunn-Edwards Paints; Desert Brand CMFPS.

Sherwin-Williams Company; Armorseal Tread-plex B90W111.

Vista Paint Corporation; Acripoxy 400.

Or Equal.

EXECUTION

EXAMINATION

Examine substrates and conditions, with Applicator present, for compliance with requirements for maximum moisture content and other conditions affecting performance of the Work.

Maximum Moisture Content of Substrates: When measured with an electronic moisture meter as follows:

Concrete: 12 percent.

Fiber-Cement Board: 12 percent.

Concrete Masonry: 12 percent.

Wood: 15 percent.

Gypsum Board: 12 percent.

Plaster: 12 percent.

Gypsum Board Substrates: Verify that finishing compound is sanded smooth.

Spray-Textured Ceiling Substrates: Verify that surfaces are dry.

Verify suitability of substrates, including surface conditions and compatibility, with existing finishes and primers.

Proceed with coating application only after unsatisfactory conditions have been corrected.

Application of coating indicates acceptance of surfaces and conditions.

PREPARATION

Comply with manufacturer's written instructions applicable to substrates and paint systems indicated.

Remove hardware, covers, plates, and similar items already in place that are removable and are not to be painted. If removal is impractical or impossible because of size or weight of item, provide surface-applied protection before surface preparation and painting.

After completing painting operations, use workers skilled in the trades involved to reinstall items that were removed. Remove surface-applied protection if any.

Clean substrates of substances that could impair bond of paints, including peeling paint, dust, dirt, oil, grease, and incompatible paints and encapsulants.

Coordination of shop-applied prime coats with topcoats is critical.

Remove incompatible primers and reprime substrate with compatible primers or apply tie coat as required to produce paint systems indicated.

Concrete Substrates: Remove release agents, curing compounds, efflorescence, and chalk. Do not paint surfaces if moisture content or alkalinity of surfaces to be painted exceeds that permitted in manufacturer's written instructions.

Concrete Masonry Substrates: Remove efflorescence and chalk. Do not paint surfaces if moisture content or alkalinity of surfaces or mortar joints exceeds that permitted in manufacturer's written instructions.

Retain "Steel Substrates" Paragraph below if steel is not shop primed or if shop primer is removed in the field.

Steel Substrates: Remove rust, loose mill scale, and shop primer, if any. Clean using methods recommended in writing by paint manufacturer, but not less than the following:

Usually retain one of first two subparagraphs below. SSPC-SP 2 and SSPC-SP 3 remove loose rust, mill scale, and paint. SSPC-SP 2 is minimum surface preparation accepted by AISC for painted steel.

SSPC-SP 2.

Retain "Shop-Primed Steel Substrates" Paragraph below if primers are shop applied and are not removed in the field.

Shop-Primed Steel Substrates: Clean field welds, bolted connections, and areas where shop paint is abraded. Paint exposed areas with the same material as used for shop priming to comply with SSPC-PA 1 for touching up shop-primed surfaces.

Galvanized-metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate surface preparation and primers.

Galvanized-Metal Substrates: Remove grease and oil residue, per SSPC-SP1, from galvanized sheet metal by mechanical methods to produce clean, lightly etched surfaces that promote adhesion of subsequently applied paints.

Wood Substrates:

Scrape and clean knots, and apply coat of knot sealer before applying primer.

Sand surfaces that will be exposed to view, and dust off.

Prime edges, ends, faces, undersides, and backsides of wood.

After priming, fill holes and imperfections in the finish surfaces with putty or plastic wood filler. Sand smooth when dried.

Gypsum Board Substrates:  Do not begin paint application until finishing compound is dry, sanded smooth, and dust free. Sand hard, slick, previously painted surfaces and remove all sanding dust.

Plaster Substrates:  Do not begin paint application until plaster is fully cured and dry.

Spray-Textured Ceiling Substrates:  Do not begin paint application until surfaces are dry.

Cotton or Canvas Insulation Covering Substrates: Remove dust, dirt, and other foreign material that might impair bond of paints to substrates.

APPLICATION

Apply paints according to manufacturer's written instructions.

If Project requires restricted application method (e.g., using only spray or rollers), revise first subparagraph below accordingly.

Use applicators and techniques suited for paint and substrate indicated.

Paint surfaces behind movable equipment and furniture same as similar exposed surfaces. Before final installation, paint surfaces behind permanently fixed equipment or furniture with prime coat only.

Paint front and backsides of access panels, removable or hinged covers, and similar hinged items to match exposed surfaces.

Do not paint over labels of independent testing agencies or equipment name, identification, performance rating, or nomenclature plates.

Primers specified in painting schedules may be omitted on items that are factory primed or factory finished if acceptable to topcoat manufacturers.

If tinting is not required, delete first paragraph below. Different tints show through as topcoat erodes.

Tint each undercoat a lighter shade to facilitate identification of each coat if multiple coats of same material are to be applied. Tint undercoats to match color of topcoat, but provide sufficient difference in shade of undercoats to distinguish each separate coat.

If undercoats or other conditions show through topcoat, apply additional coats until cured film has a uniform paint finish, color, and appearance.

Apply paints to produce surface films without cloudiness, spotting, holidays, laps, brush marks, roller tracking, runs, sags, ropiness, or other surface imperfections. Cut in sharp lines and color breaks.

Painting Fire Suppression, Plumbing, HVAC, Electrical, Communication, and Electronic Safety and Security Work:

Paint the following work where exposed in equipment rooms:

List below contains items that are often field painted, plus others that are often not. Revise list to suit Project.

Equipment, including panelboards[ and switch gear].

Uninsulated metal piping.

Uninsulated plastic piping.

Pipe hangers and supports.

Metal conduit.

Plastic conduit.

Tanks that do not have factory-applied final finishes.

Duct, equipment, and pipe insulation having cotton or canvas insulation covering or other paintable jacket material.

Mechanical equipment that is indicated to have factory-primed finish for field painting.

Electrical equipment that is indicated to have a factory-primed finish for field painting.

Paint the following work where exposed in occupied spaces:

List below contains items that are usually field painted. Revise list to suit Project.

Equipment, including panelboards.

Uninsulated metal piping.

Uninsulated plastic piping.

Pipe hangers and supports.

Metal conduit.

Plastic conduit.

Duct, equipment, and pipe insulation having cotton or canvas insulation covering or other paintable jacket material.

Other items as directed by Architect.

Paint portions of internal surfaces of metal ducts, without liner, behind air inlets and outlets that are visible from occupied spaces.

FIELD QUALITY CONTROL

Dry Film Thickness Testing: District may engage the services of a qualified testing and inspecting agency to inspect and test paint for dry film thickness.

Contractor shall touch up and restore painted surfaces damaged by testing.

If test results show that dry film thickness of applied paint does not comply with paint manufacturer's written recommendations, Contractor shall pay for testing and apply additional coats as needed to provide dry film thickness that complies with paint manufacturer's written recommendations.

CLEANING AND PROTECTION

At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

After completing paint application, clean spattered surfaces. Remove spattered paints by washing, scraping, or other methods. Do not scratch or damage adjacent finished surfaces.

Protect work of other trades against damage from paint application. Correct damage to work of other trades by cleaning, repairing, replacing, and refinishing, as approved by Architect, and leave in an undamaged condition.

At completion of construction activities of other trades, touch up and restore damaged or defaced painted surfaces.

Determine the appropriate finish levels (flat, semigloss, gloss) for the specific applications.  Consider selecting Semigloss paint for most applications.

INTERIOR PAINTING SCHEDULE

Concrete Substrates, Nontraffic Surfaces:

Institutional Low-Odor/VOC Latex System:

Prime Coat: Interior Latex Primer/Sealer for concrete, plaster and porous surfaces.

Intermediate Coat: Interior Acrylic Latex.

Topcoat: Interior Acrylic Latex, [flat] [eggshell] [semigloss].

Concrete Substrates, Traffic Surfaces:

Latex Floor Enamel System:

Prime Coat: Latex Floor Enamel.

Topcoat: Latex Floor Enamel.

Water-Based Clear Sealer System:

Prime Coat:  Interior/Exterior clear concrete floor sealer (water based).

Topcoat:  Interior/Exterior clear concrete floor sealer (water based).

CMU Substrates:

Institutional Low-Odor/VOC Latex System:

Block Filler/Prime Coat: Interior/Exterior Latex Block Filler.

Intermediate Coat: Interior Acrylic Latex.

Topcoat: Interior Acrylic Latex.

Steel Substrates:

Latex System:

Prime Coat:Acrylic Ferrous Metal Primer.

Intermediate Coat: Primer, Interior Acrylic Latex.

Topcoat: Interior Acrylid Latex.

Galvanized-metal substrates should not be chromate passivated if primer is field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate surface preparation and primers.

Galvanized-Metal and Non-Ferrous Substrates:

Latex System:

Pretreatment:  Non-Ferrous Metal Pretreatment.

Prime Coat:  Acrylic Non-Ferrous Metal Primer.

Topcoat:  Two coats of Interior Acrylic.

Wood Substrates: Glued-laminated construction.

Latex System:

Prime Coat: Interior Latex Wood Primer.

Intermediate Coat: Interior Acrylic Latex.

Topcoat:  Interior Acrylic Latex.

Wood Substrates: Exposed framing.

Latex System:

Prime Coat: Interior Latex Wood Primer.

Intermediate Coat: Interior Acrylic Latex.

Topcoat:  Interior Acrylic Latex.

Wood Substrates: Wood trim; Architectural woodwork; Doors Wood paneling; and casework.

Latex System:

Prime Coat: Interior Latex Wood Primer.

Intermediate Coat: Interior Acrylic Latex.

Topcoat:  Interior Acrylic Latex.

Gypsum Board Substrates:

Institutional Low-Odor/VOC Latex System:

Prime Coat: Interior Latex Primer/Sealer for gypsum board.

Intermediate Coat:  Interior Acrylic Latex.

Top Coat: Interior Acrylic Latex.

Cotton or Canvas and ASJ Insulation-Covering Substrates: Including pipe and duct

- coverings.

Latex System:

Prime Coat: Interior Latex Primer/Sealer.

Intermediate Coat: Interior Latex, (matching topcoat).

Topcoat: Latex Dry Fog/Fall or flat.

END OF SECTION 09 91 23

Retain this notice in all Sections of Project Manual.

San Diego Unified School District Guide Specifications

Document Version: August 2021