MasterSpec 2012

SECTION 31 63 29

DRILLED CONCRETE PIERS AND SHAFTS

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

GENERAL

RELATED DOCUMENTS

MANDATORY REQUIREMENT:  Retain this article in all Sections of Project Manual.

Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

SUMMARY

Section Includes:

Dry-installed drilled piers.

UNIT PRICES

Retain this article if Work specified in this Section is measured and paid for under the provisions of unit prices. Do not include amounts. Insert descriptions of items in Part 2 or 3 to provide information affecting the cost of the Work that is not included under the unit price.

Drilled Piers: Actual net volume of drilled piers in place and approved in addition to that indicated on drawings.

Separate unit-price items for shaft and bell volumes, if applicable, because costs of belling are much higher than shaft construction.

Unit prices include labor, materials, tools, equipment, and incidentals required for excavation, trimming, shoring, casings, dewatering, reinforcement, concrete fill, testing and inspecting, and other items for complete drilled-pier installation.

No additional compensation will be made for excavation, concrete fill, reinforcement, casings, or other costs due to unauthorized over excavating of shafts or bells.

Retain "Rock Measurement" Paragraph below for classified excavation.

Rock Measurement: Volume of rock actually removed, measured in original position, but not to exceed outside dimensions of drilled piers cast against rock. Unit prices for rock excavation include replacement with approved materials.

PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

Preinstallation Conference: Conduct conference at Project site.

Retain subparagraph below if additional requirements are necessary; include information about conference.

Review methods and procedures related to drilled piers, including:

Review geotechnical report.

Discuss existing utilities and subsurface conditions.

Review coordination with temporary controls and protections.

Review measurement and payment of unit prices.

If needed, insert list of conference participants not mentioned in Section 01 31 00 "Project Management and Coordination."

ACTION SUBMITTALS

Product Data: For each type of product.

Design Mixtures: For each concrete mixture. Submit alternative design mixtures when characteristics of materials, Project conditions, weather, test results, or other circumstances warrant adjustments.

Indicate amounts of mixing water to be withheld for later addition at Project site.

Retain "Shop Drawings" Paragraph below if drilled piers are reinforced.

Shop Drawings: For concrete reinforcement, detailing fabricating, bending, supporting, and placing.

INFORMATIONAL SUBMITTALS

Coordinate "Qualification Data" Paragraph below with qualification requirements in "Quality Assurance" Article.

Qualification Data: For Installer [land surveyor] [professional engineer].

Retain "Welding certificates" Paragraph below if retaining "Welding Qualifications" Paragraph in "Quality Assurance" Article.

Welding certificates.

Retain "Material Certificates" Paragraph below to require submittal of material certificates from manufacturers.

Material Certificates: From manufacturer, for the following:

Cementitious materials.

Admixtures.

Steel reinforcement and accessories.

Retain "Material Test Reports" Paragraph below for material test reports that are Contractor's responsibility.

Material Test Reports: For each material below, by a qualified testing agency:

Aggregates: Include service record data indicating absence of deleterious expansion of concrete due to alkali aggregate reactivity.

CLOSEOUT SUBMITTALS

Coordinate this article with Section 01 77 00 "Closeout Procedures" and with Section 01 78 39 "Project Record Documents."

Record drawings.

QUALITY ASSURANCE

Installer Qualifications: An experienced installer that has specialized in drilled-pier work.

Retain "Welding Qualifications" Paragraph below if shop or field welding is required. If retaining, also retain "Welding certificates" Paragraph in "Informational Submittals" Article.

Welding Qualifications: Qualify procedures and personnel according to the following:

AWS D1.1/D1.1M, "Structural Welding Code - Steel."

AWS D1.4/D1.4M, "Structural Welding Code - Reinforcing Steel."

FIELD CONDITIONS

Existing Utilities: Locate existing underground utilities before excavating drilled piers. If utilities are to remain in place, provide protection from damage during drilled-pier operations.

Should uncharted or incorrectly charted piping or other utilities be encountered during excavation, adapt drilling procedure if necessary to prevent damage to utilities. Cooperate with District and utility companies in keeping services and facilities in operation without interruption. Repair damaged utilities to satisfaction of utility owner.

Retain "Interruption of Existing Utilities" Paragraph below if interruption of existing utility service is required.

Interruption of Existing Utilities: Do not interrupt any utility to facilities occupied by District or others unless permitted under the following conditions and then only after arranging to provide temporary utility according to requirements indicated:

Notify District Construction Manager no fewer than seven days in advance of proposed interruption of utility.

Do not proceed with interruption of utility without District Construction Manager’s written permission.

Project-Site Information: A geotechnical report has been prepared for this Project and is available for information only. The report is not part of the Contract Documents. The opinions expressed in this report are those of geotechnical engineer and represent interpretations of subsoil conditions, tests, and results of analyses conducted by geotechnical engineer. The District is not responsible for interpretations or conclusions drawn from this data.

Make additional test borings and conduct other exploratory operations necessary for drilled piers.

The geotechnical report is available from the District Construction Manager.

Coordinate "Survey Work" Paragraph below with Section 01 73 00 "Execution."

Survey Work: Engage a qualified land surveyor or professional engineer to perform surveys, layouts, and measurements for drilled piers. Before excavating, lay out each drilled pier to lines and levels required. Record actual measurements of each drilled pier's location, shaft diameter, bottom and top elevations, deviations from specified tolerances, and other specified data.

Record and maintain information pertinent to each drilled pier and indicate on record Drawings. Cooperate with District's testing and inspecting agency to provide data for required reports.

PRODUCTS

PERFORMANCE REQUIREMENTS

Drilled-Pier Standard: Comply with ACI 336.1, “Specification for the Construction of Drilled Piers”, except as modified in this Section.

STEEL REINFORCEMENT

Retain this article if reinforced-concrete drilled piers are used. Retain type and grade of reinforcement required or revise to suit Project. See the Evaluations in Section 03 30 00 "Cast-in-Place Concrete" for discussion of steel reinforcement.

Reinforcing Bars: ASTM A 615/A 615M, Grade 60, deformed.

Retain "Epoxy-Coated Reinforcing Bars" Paragraph below for epoxy-coated steel reinforcement. Retain type of reinforcement from first set of options; retain epoxy-coated product from second set. ASTM A 775/A 775M bars are usually epoxy coated before fabrication; ASTM A 934/A 934M bars are epoxy coated after fabrication and should not be field bent or rebent.

Epoxy-Coated Reinforcing Bars: [ASTM A 615/A 615M, Grade 60] [ASTM A 706/A 706M], deformed bars, [ASTM A 775/A 775M] [or] [ASTM A 934/A 934M], epoxy coated, with less than 2 percent damaged coating in each 12-inch bar length.

Plain-Steel Wire: ASTM A 82/A 82M, [as drawn] [galvanized].

Deformed-Steel Wire: ASTM A 496/A 496M.

Epoxy-Coated Wire: ASTM A 884/A 884M, Class A, Type 1 coated, [as-drawn, plain] [deformed]-steel wire, with less than 2 percent damaged coating in each 12-inch wire length.

Insert other products for dowels or dowel sleeves if required. See Section 03 30 00 "Cast-in-Place Concrete."

Joint Dowel Bars: ASTM A 615/A 615M, Grade 60, plain. Cut bars true to length with ends square and free of burrs.

CONCRETE MATERIALS

See the Evaluations in Section 03 30 00 "Cast-in-Place Concrete" for discussion of concrete materials.

Cementitious Material: Use the following cementitious materials, of same type, brand, and source, throughout Project:

Retain type of portland cement from options in "Portland Cement" Subparagraph below. ACI 336.1 limits portland cement to Type I or II.

Portland Cement: ASTM C 150/C 150M, [Type I] [Type II][Type V].[ Supplement with the following:]

Fly Ash: ASTM C 618, Class F.

Insert aggregate class from ASTM C 33/C 33M or aggregate gradation in "Normal-Weight Aggregate" Paragraph below if required. Retain last option below if damage caused by concrete expansion from alkali silica or alkali carbonate reactions is anticipated.

Normal-Weight Aggregate: ASTM C 33/C 33M, graded, 3/4-inch-nominal maximum coarse-aggregate size. Provide aggregate from a single source with documented service record data of at least 5 years' satisfactory service in similar applications and service conditions using similar aggregates and cementitious materials.

Retain "Fine Aggregate" Subparagraph below if optional restriction for fine aggregate in ASTM C 33/C 33M is required.

Fine Aggregate: Free of materials with deleterious reactivity to alkali in cement.

Water: ASTM C 94/C 94M and potable.

Chemical Admixtures: Provide admixtures certified by manufacturer to be compatible with other admixtures and that do not contribute water-soluble chloride ions exceeding those permitted in hardened concrete. Do not use calcium chloride or admixtures containing calcium chloride.

Retain one or more chemical admixtures from first four subparagraphs below.

Water-Reducing Admixture: ASTM C 494/C 494M, Type A.

Water-Reducing and Retarding Admixture: ASTM C 494/C 494M, Type D.

High-Range, Water-Reducing and Retarding Admixture: ASTM C 494/C 494M, Type G.

Plasticizing and Retarding Admixture: ASTM C 1017/C 1017M, Type II.

Compressive strength of grout mix in "Sand-Cement Grout" Paragraph below is based on the "Optional Requirements Checklist" accompanying ACI 336.1. Grout is used to fill any visible voids and the annular space between permanent casing and shaft wall or between permanent liner and oversized temporary casing.

Sand-Cement Grout: Portland cement, ASTM C 150/C 150M, Type II; clean natural sand, ASTM C 404; and water to result in grout with a minimum 28-day compressive strength of 1000 psi, of consistency required for application.

STEEL CASINGS

Retain this article if permanent steel casings are required. Retain type of casing from "Steel Pipe Casings" and "Corrugated-Steel Pipe Casings" paragraphs below.

Steel Pipe Casings: ASTM A 283/A 283M, Grade C, or ASTM A 36/A 36M, carbon-steel plate, with joints full-penetration welded according to AWS D1.1/D1.1M.

Corrugated-Steel Pipe Casings: ASTM A 929/A 929M, steel sheet, zinc coated.

Retain "Liners" Paragraph below if liners are required to suit Project.

Liners: Comply with ACI 336.1.

CONCRETE MIXTURES

Prepare design mixtures for each type and strength of concrete, proportioned on the basis of laboratory trial mixture or field test data, or both, according to ACI 301.

Limit use of fly ash and silica fume to not exceed 15% of weight of Portland Cement.

Cementitious Materials: Limit percentage, by weight, of cementitious materials other than Portland cement according to ACI 301 limits as if concrete were exposed to deicing chemicals.

Retain first option in first paragraph below if drilled piers are exposed to chlorides in service; retain second option for situations that are not dry or protected from moisture in service. Percentages are from ACI 301 (ACI 301M).

Limit water-soluble, chloride-ion content in hardened concrete to [0.15] [0.30] percent by weight of cement.

If different concrete mixtures are required, copy paragraph below and re-edit to suit Project; indicate locations of each concrete mixture here or on Drawings.

Proportion normal-weight concrete mixture as follows:

Retain strength from six options in "Compressive Strength (28 Days)" Subparagraph below. Coordinate compressive strength with water-cementitious materials ratio if concrete is subject to special exposure conditions or sulfate exposure.

Compressive Strength (28 Days): [6000 psi] [5000 psi] [4500 psi] [4000 psi] [3500 psi] [3000 psi].

Retain water-cementitious materials ratio from three options in "Maximum Water-Cementitious Materials Ratio" Subparagraph below or revise to suit Project; delete if in-service durability conditions are benign and limits on water-cementitious materials ratio are not required. Coordinate water-cementitious materials ratio with compressive strength.

Maximum Water-Cementitious Materials Ratio: [0.50] [0.45] [0.40].

Minimum Slump: Capable of maintaining the following slump until completion of placement:

Minimum slump in first three subparagraphs below is based on ACI 336.1. Retain applicable subparagraphs for drilling methods permitted. Revise to insert slump limit if applicable; ACI 336.1 sets no upper slump limit.

4 inches for dry, uncased, or permanent-cased drilling method.

6 inches for temporary-casing drilling method.

Air Content: Do not air entrain concrete.

REINFORCEMENT FABRICATION

Fabricate steel reinforcement according to CRSI's "Manual of Standard Practice."

CONCRETE MIXING

Ready-Mixed Concrete: Measure, batch, mix, and deliver concrete according to ASTM C 94/C 94M, and furnish batch ticket information.

When air temperature is between 85 and 90 deg F, reduce mixing and delivery time from 1-1/2 hours to 75 minutes; when air temperature is above 90 deg F, reduce mixing and delivery time to 60 minutes.

EXECUTION

PREPARATION

Protect structures, utilities, sidewalks, pavements, and other facilities from damage caused by settlement, lateral movement, vibration, and other hazards created by drilled-pier operations.

EXCAVATION

Classified Excavation: Excavation is classified as standard excavation, special excavation, and obstruction removal and includes excavation to bearing elevations as follows:

In first subparagraph below, insert geotechnical engineer's recommended minimum values for power, torque, and downthrust of drilling equipment if required.

Standard excavation includes excavation accomplished with conventional augers fitted with soil or rock teeth, drilling buckets, or underreaming tools attached to drilling equipment of size, power, torque, and downthrust necessary for the Work.

Rock properties in first subparagraph below could be defined by specifying a maximum rate of penetration to define refusal.

Special excavation includes excavation that requires special equipment or procedures where drilled-pier excavation equipment used in standard excavation, operating at maximum power, torque, and downthrust, cannot advance the shaft.

Special excavation requires use of special rock augers, core barrels, air tools, blasting, or other methods of hand excavation.

Earth seams, rock fragments, and voids included in rock excavation area are considered rock for full volume of shaft from initial contact with rock.

Obstructions: Payment for removing unanticipated boulders, concrete, masonry, or other subsurface obstructions that cannot be removed by conventional augers fitted with soil or rock teeth, drilling buckets, or underreaming tools attached to drilling equipment of size, power, torque, and downthrust necessary for the Work is according to Contract provisions for changes in the Work.

Dewatering: Prevent surface water from entering excavated shafts. Dewater excavated shafts prior to concrete work. Conduct water to site drainage facilities.

Excavate shafts for drilled piers to indicated elevations. Remove loose material from bottom of excavation.

Retain applicable subparagraphs below.

Excavate bottom of drilled piers to level plane within 1:12 tolerance.

Remove water from excavated shafts before concreting.

Retain first subparagraph below if socketing drilled pier into rock.

Excavate rock sockets of dimensions indicated.

Retain subparagraph below if grooving lower portions of shaft to develop side resistance.

Cut series of grooves about perimeter of shaft to height from bottom of shaft, vertical spacing, and dimensions indicated.

Insert new paragraph here if anticipating that some drilled piers might reach suitable bearing at depths above elevations indicated. Insert criteria that define suitable bearing strength of strata, such as minimum compressive strength, penetrometer, or shear strength tests.

Notify and allow testing and inspecting agency to test and inspect bottom of excavation. If unsuitable bearing stratum is encountered, make adjustments to drilled piers as determined by the District Construction Manager.

Do not excavate shafts deeper than elevations indicated unless approved by the District Construction Manager.

Payment for additional authorized excavation is according to Contract provisions for changes in the Work.

Retain first "End-Bearing Drilled Piers" Paragraph below if further exploration below bearing elevation is required for end-bearing piers or if soft soils are suspected. Use of auger probe varies regionally. Delete or revise depth of probe if water-bearing strata may be encountered.

End-Bearing Drilled Piers: Probe with auger to a depth below bearing elevation, equal to diameter of the bearing area of drilled pier. Determine whether voids, clay seams, or solution channels exist.

Revise frequency of tests in first subparagraph below to suit Project.

Test first three drilled piers and one of every six drilled piers thereafter.

Fill augur-probe holes with grout.

Retain "End-Bearing Drilled Piers" Paragraph below if drilled piers bear on clay or hardpan.

End-Bearing Drilled Piers: Probe with auger to a depth of 96 inches below bottom elevation of shaft, and visually inspect and classify soil. Verify continuity and thickness of strata.

Revise frequency of tests in subparagraph below to suit Project.

Test first three drilled piers and one of every six drilled piers thereafter.

If retaining first paragraph below, revise to state minimum spacing determined by geotechnical engineer.

Excavate shafts for closely spaced drilled piers and for drilled piers occurring in fragile or sand strata only after adjacent drilled piers are filled with concrete and allowed to set.

Retain "Temporary Casings" Paragraph below if permanent casings are not required. Temporary casings may not be required if permanent casings are not used.

Temporary Casings: Install watertight steel casings of sufficient length and thickness to prevent water seepage into shaft; to withstand compressive, displacement, and withdrawal stresses; and to maintain stability of shaft walls.

Remove temporary casings, maintained in plumb position, during concrete placement and before initial set of concrete[, or leave temporary casings in place].

Retain "Bells" Paragraph below if bells are required. Examine soil stability and constructability before designing drilled piers with bells.

Bells: Excavate bells for drilled piers to shape, base thickness, and slope angle indicated. Excavate bottom of bells to level plane and remove loose material before placing concrete.

Retain subparagraph below if shoring of bells is necessary or practical.

Shore bells in unstable soil conditions to prevent cave-in during excavation, inspection, and concreting.

Review ACI 336.1 tolerances and revise "Tolerances" Paragraph below to insert exceptions if applicable.

Tolerances: Construct drilled piers to remain within ACI 336.1 tolerances.

If location or out-of-plumb tolerances are exceeded, provide corrective construction. Submit corrective construction proposals to District Construction Manager for review before proceeding.

Inspection: Each drilled pier will be inspected and tested by the District’s testing agency prior to placing concrete.

Provide and maintain facilities with equipment required for testing and inspecting excavations.  Cooperate with testing and inspecting personnel to expedite the Work.

Notify District Construction Manager at least 24 hours before excavations are ready for tests and inspection.

PERMANENT STEEL CASING INSTALLATION

Retain this article if installing permanent casings by dry method.

Install permanent steel casings of minimum wall thickness indicated and of diameter not less than diameter of drilled pier.

Install casings as excavation proceeds, to maintain sidewall stability.

Retain first subparagraph below if casing is seated into rock stratum. Delete if corrugated-steel casing is selected.

Fabricate bottom edge of lowest casing section with cutting shoe capable of penetrating rock and achieving water seal.

Connect casing sections by continuous penetration welds to form watertight, continuous casing.

Remove and replace or repair casings that have been damaged during installation and that could impair strength or efficiency of drilled pier.

Revise subparagraph below if high-slump concrete is permitted.

Fill annular void between casing and shaft wall with grout.

Delete "Corrugated-Steel Casings" Paragraph below if steel pipe casings are used; corrugated-steel casings may not be watertight installations.

Corrugated-Steel Casings: Provide corrugated-steel casings formed from zinc-coated steel sheet.

Corrugated casings may be delivered in sections or panels of convenient length and field connected according to manufacturer's written instructions.

STEEL REINFORCEMENT INSTALLATION

Retain this article if reinforcement is required.

Comply with recommendations in CRSI's "Manual of Standard Practice" for fabricating, placing, and supporting reinforcement.

Clean reinforcement of loose rust and mill scale, earth, and other materials that reduce or destroy bond with concrete.

Fabricate and install reinforcing cages symmetrically about axis of shafts in a single unit.

Accurately position, support, and secure reinforcement against displacement during concreting. Maintain minimum cover over reinforcement.

Use templates to set anchor bolts, leveling plates, and other accessories furnished in work of other Sections. Provide blocking and holding devices to maintain required position during final concrete placement.

Protect exposed ends of extended reinforcement, dowels, or anchor bolts from mechanical damage and exposure to weather.

CONCRETE PLACEMENT

Place concrete in continuous operation and without segregation immediately after inspection and approval of shaft by a qualified Special Inspector.

Revise methods or restrictions in "Dry Method" Paragraph below to suit Project. ACI 336.1 permits free-fall concreting, but in its "Optional Requirements Checklist" it cautions against permitting free-fall concreting for pier diameters less than 30 inches (750 mm). Insert any special requirements for tremie placement or pumping concrete if free-fall concrete is unacceptable.

Dry Method: Place concrete to fall vertically down the center of drilled pier without striking sides of shaft or steel reinforcement.

Where concrete cannot be directed down shaft without striking reinforcement, place concrete with chutes, tremies, or pumps.

Vibrate top 60 inches of concrete.

Coordinate withdrawal of temporary casings with concrete placement to maintain at least a 60-inch head of concrete above bottom of casing.

Vibrate top 60 inches of concrete after withdrawal of temporary casing.

Screed concrete at cutoff elevation level and apply scoured, rough finish. Where cutoff elevation is above the ground elevation, form top section above grade and extend shaft to required elevation.

Protect concrete work, according to ACI 301, from frost, freezing, or low temperatures that could cause physical damage or reduced strength.

Do not use calcium chloride, salt, or other mineral-containing antifreeze agents or chemical accelerators.

If hot-weather conditions exist that would seriously impair quality and strength of concrete, place concrete according to ACI 301 to maintain delivered temperature of concrete at no more than 90 deg F.

Retain subparagraph below if significant exposure of portions of drilled piers is expected.

Place concrete immediately on delivery. Keep exposed concrete surfaces and formed shaft extensions moist by fog sprays, wet burlap, or other effective means for a minimum of seven days.

FIELD QUALITY CONTROL

Special Inspections: District will engage a qualified special inspector to perform the following special inspections:

Drilled piers.

Excavation.

Concrete.

Steel reinforcement welding.

Testing Agency: District will engage a qualified testing agency to perform tests and inspections.

Retain "Drilled-Pier Tests and Inspections" Paragraph below to describe tests and inspections to be performed.

See Section 01 40 01 "Quality Requirements / District Laboratory" for retesting and reinspecting requirements and Section 01 73 00 "Execution" for requirements for correcting the Work.

An excavation, concrete, or a drilled pier will be considered defective if it does not pass tests and inspections.

DISPOSAL OF SURPLUS AND WASTE MATERIALS

Disposal: Remove surplus satisfactory soil and waste material, including unsatisfactory soil, trash, and debris, and legally dispose of it off District's property.

END OF SECTION 31 63 29

Retain this notice in all Sections of Project Manual.

San Diego Unified School District Guide Specifications

Document Version: August 2021