MasterSpec 2012

SECTION 32 13 73

CONCRETE PAVING JOINT SEALANTS

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

GENERAL

RELATED DOCUMENTS

MANDATORY REQUIREMENT:  Retain this article in all Sections of Project Manual.

Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

SUMMARY

Section Includes:

Expansion and contraction joints within Portland cement concrete pavement.

Cold-applied joint sealants.

Joint-sealant backer materials.

Primers.

ACTION SUBMITTALS

Product Data:  For each type of product.

INFORMATIONAL SUBMITTALS

Product Certificates:  For each type of joint sealant and accessory.

DELIVERY, STORAGE, AND HANDLING

Deliver materials to Project site in original unopened containers or bundles with labels indicating manufacturer, product name and designation, color, expiration date, pot life, curing time, and mixing instructions for multicomponent materials.

Store and handle materials to comply with manufacturer's written instructions to prevent their deterioration or damage due to moisture, high or low temperatures, contaminants, or other causes.

FIELD CONDITIONS

Do not proceed with installation of joint sealants under the following conditions:

When ambient and substrate temperature conditions are outside limits permitted by joint-sealant manufacturer or are below 40 deg F.

When joint substrates are wet.

Where joint widths are less than those allowed by joint-sealant manufacturer for applications indicated.

Where contaminants capable of interfering with adhesion have not yet been removed from joint substrates.

PRODUCTS

MATERIALS, GENERAL

Compatibility: Provide joint sealants, backing materials, and other related materials that are compatible with one another and with joint substrates under conditions of service and application, as demonstrated by joint-sealant manufacturer, based on testing and field experience.

Colors of Exposed Joint Sealants:  As selected by Architect from manufacturer's full range for this characteristic.

COLD-APPLIED JOINT SEALANTS

Single-Component, Nonsag, Low-Modulus, Neutral-Curing, Silicone Joint Sealant for Concrete:  ASTM D 5893/D 5893M, Type NS.

Manufacturers:  Subject to compliance with requirements, provide products by one of the following:

Roadsaver Silicone-SL; Crafco Inc.

888; Dow Corning Corporation.

Pecora Corporation.

Or Equal.

Multicomponent, Pourable, Urethane, Chemically Curing Elastomeric Formulation Jet-Fuel-Resistant Joint Sealant for Concrete: ASTM C 920; Type M; Grade P; Class 12-1/2; for Uses T, M, and, as applicable to joint substrates indicated, O.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Vulkem 202; Mameco International.

Urexpan NR-300; Pecora Corporation.

Sealtight Gardox; W. R. Meadows, Inc.

Or Equal.

JOINT-SEALANT BACKER MATERIALS

Joint-Sealant Backer Materials: Nonstaining; compatible with joint substrates, sealants, primers, and other joint fillers; and approved for applications indicated by joint-sealant manufacturer, based on field experience and laboratory testing.

Retain "Round Backer Rods for Cold-Applied Joint Sealants" Paragraph below for use in joints such as contraction joints cut partially through paving material.

Round Backer Rods for Cold-Applied Joint Sealants:  ASTM D 5249, Type 3, of diameter and density required to control joint-sealant depth and prevent bottom-side adhesion of sealant.

Retain "Backer Strips for Cold-Applied Joint Sealants" Paragraph below for use in joints extending through the full depth of the paving.

Backer Strips for Cold-Applied Joint Sealants: ASTM D 5249; Type 2; of thickness and width required to control joint-sealant depth, prevent bottom-side adhesion of sealant, and fill remainder of joint opening under sealant.

PRIMERS

Primers:  Product recommended by joint-sealant manufacturer where required for adhesion of sealant to joint substrates indicated, as determined from pre-installation joint-sealant-substrate tests and field tests.

EXECUTION

EXAMINATION

Examine joints to receive joint sealants, with Installer present, for compliance with requirements for joint configuration, installation tolerances, and other conditions affecting joint-sealant performance.

Proceed with installation only after unsatisfactory conditions have been corrected.

PREPARATION

Surface Cleaning of Joints:  Clean out joints immediately before installing joint sealants to comply with joint-sealant manufacturer's written instructions.

Remove all foreign material from joint substrates that could interfere with adhesion of joint sealant, including dust, old joint sealants, oil, grease, waterproofing, water repellents, water, surface dirt, and frost.

Joint Priming: Prime joint substrates where indicated or where recommended in writing by joint-sealant manufacturer, based on pre-installation joint-sealant-substrate tests or prior experience. Apply primer to comply with joint-sealant manufacturer's written instructions. Confine primers to areas of joint-sealant bond; do not allow spillage or migration onto adjoining surfaces.

INSTALLATION OF JOINT SEALANTS

Comply with joint-sealant manufacturer's written installation instructions for products and applications indicated unless more stringent requirements apply.

Joint-Sealant Installation Standard: Comply with recommendations in ASTM C 1193 for use of joint sealants as applicable to materials, applications, and conditions.

Install joint-sealant backings to support joint sealants during application and at position required to produce cross-sectional shapes and depths of installed sealants relative to joint widths that allow optimum sealant movement capability.

Do not leave gaps between ends of joint-sealant backings.

Do not stretch, twist, puncture, or tear joint-sealant backings.

Remove absorbent joint-sealant backings that have become wet before sealant application and replace them with dry materials.

Install joint sealants immediately following backing installation, using proven techniques that comply with the following:

Place joint sealants so they fully contact joint substrates.

Completely fill recesses in each joint configuration.

Produce uniform, cross-sectional shapes and depths relative to joint widths that allow optimum sealant movement capability.

Tooling of Nonsag Joint Sealants: Immediately after joint-sealant application and before skinning or curing begins, tool sealants according to the following requirements to form smooth, uniform beads of configuration indicated; to eliminate air pockets; and to ensure contact and adhesion of sealant with sides of joint:

Remove excess joint sealant from surfaces adjacent to joints.

Use tooling agents that are approved in writing by joint-sealant manufacturer and that do not discolor sealants or adjacent surfaces.

Provide joint configuration to comply with joint-sealant manufacturer's written instructions unless otherwise indicated.

CLEANING AND PROTECTION

Clean off excess joint sealant as the Work progresses, by methods and with cleaning materials approved in writing by joint-sealant manufacturers.

Protect joint sealants, during and after curing period, from contact with contaminating substances and from damage resulting from construction operations or other causes so sealants are without deterioration or damage at time of Substantial Completion. If, despite such protection, damage or deterioration occurs, cut out and remove damaged or deteriorated joint sealants immediately and replace with joint sealant so installations in repaired areas are indistinguishable from the original work.

END OF SECTION 32 13 73

Retain this notice in all Sections of Project Manual.

San Diego Unified School District Guide Specifications

Document Version: August 2021