MasterSpec Template

SECTION 32 15 40.01

DECOMPOSED GRANITE SURFACING

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

GENERAL

RELATED DOCUMENTS

MANDATORY REQUIREMENT:  Retain this article in all Sections of Project Manual.

Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

SUMMARY

Section includes decomposed granite (DG) surfacing.

Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

Section 01 40 01 "Quality Requirements – District Laboratory" for compaction testing.

Section 31 20 00 "Earth Moving" for subgrade preparation.

Section 32 92 00 "Turf and Grasses" and Section 32 93 00 "Plants” for coordinating timing of maintenance period.

DEFINITIONS

Retain terms that remain after this Section has been edited for a project.  Show locations of each type of DG on Drawings.  Use stabilized granite everywhere except 1) when used as ground cover in planting areas, 2) within 5 feet of tree trunks in tree planters.

Decomposed Granite (DG): Non-stabilized aggregate surfacing materials as specified herein.

Stabilized DG: DG that is stabilized by adding binder to the aggregate mixture.

ACTION SUBMITTALS

Product Data: For each type of product.

Samples for Color Verification: For all proposed aggregates:

Quantity: 5 pounds

Samples for Analysis and Verification: For aggregates proposed for use in stabilized DG surfacing areas:

After color verification samples have been approved, submit two identical samples: One to Architect and the other to binder manufacturer.

Quantity: 5 pounds.

Include aggregate supplier’s sieve analysis for grading.

Allow two weeks processing time for binder manufacturer to perform additional analysis to determine blending formula.

Submit binder manufacturer’s blending formula to District Construction Manager for approval.

INFORMATIONAL SUBMITTALS

Coordinate "Qualification Data" Paragraph below with qualification requirements in "Quality Assurance" Article.

Qualification Data: For installer.

Manufacturer Certificates: Material Certificates: Signed by suppliers certifying that each material complies with requirements.

CLOSEOUT SUBMITTALS

Maintenance Data: For stabilized DG surfacing to include in maintenance manuals.

QUALITY ASSURANCE

Stabilized DG Surfacing Installer Qualifications:  Installer shall have five years successful experience with projects of similar scope and design.

Stabilized DG Surfacing Mockup:

Build mockup to verify selections made under Sample submittals and to demonstrate aesthetic effects and set quality standards for fabrication and installation.

Construction of mock-up shall be the same as construction indicated on Drawings and in specifications.

Size: Approximately four feet by 10 feet by full thickness, including base.

Include edging.

Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless District Construction Manager specifically approves such deviations in writing.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 01 40 02 "Quality Requirements / Contractor Laboratory" for demolishing and removing mockups.

Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

DELIVERY, STORAGE, AND HANDLING

Bulk Materials:

Accompany each delivery of bulk materials with appropriate certificates.

Do not dump or store bulk materials near structures, utilities, walkways and pavements, or on existing turf areas or plants.

Do not move or handle materials when they are wet.

Protect bulk materials from erosion.  Provide erosion-control measures to prevent erosion or displacement of bulk materials, discharge of soil-bearing water runoff and airborne dust reaching adjacent properties, water conveyance systems, or walkways.

Packaged Materials: Deliver packaged materials in original, unopened containers showing weight, name and address of manufacturer, and compliance with state and Federal laws if applicable.

FIELD CONDITIONS

Weather Limitations: Proceed with installation only when existing and forecasted weather conditions permit DG and stabilized DG surfacing to be installed according to manufacturer's written instructions.  Do not install during rainy conditions or when temperature is below 40 degrees Fahrenheit and falling.

PRODUCTS

AGGREGATE MATERIALS

Igneous rock which has weathered in place or any sedimentary material principally derived from igneous rock.

Base: CalTrans Class II crushed granular road base.

Provide washed material free of organic material and other deleterious substances.

C-35, crushed 3/8” minus or 1/4” minus conforming to the following gradation as determined by ASTM C 136:

| - Sieve Size | - Percent Passing (by weight) |
| --- | --- |
| - 3/8 inch | - 100 |
| - No. 4 | - 100 |
| - No. 8 | - 93 |
| - No. 16 | - 65 |
| - No. 30 | - 44 |
| - No. 50 | - 28 |
| - No. 100 | - 16 |
| - No. 200 | - 8.7 |
| - Resistance “R” value 82% |  |
| - Sand equivalent value 61% |  |

BINDER

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Stabilizer as distributed by Stabilizer Solutions, Inc.

Natracil as distributed by Gail Materials.

Or Equal.

Description: Colorless, odorless, non-toxic, organic polymer derived from psyllium husk, in concentrated powder form.

EDGING

Wood Edging:  Wood edging and stakes of sizes shown and of the following wood species:

Species:  Foundation Grade redwood.

Size:  2 x 6 unless otherwise indicated.

Stakes:  Wood, same species, 1 x 2 by 18 inches long in nominal size with galvanized nails for anchoring headers and edging.

EXECUTION

EXAMINATION

Examine areas to receive DG surfacing, with Installer present, for compliance with requirements and conditions affecting installation and performance of the Work.

Where surfacing is indicated to fit with other construction, verify dimensions of other construction by field measurements before proceeding with the Work.

Verify that subgrade is dry and in suitable condition to support surfacing and imposed loads.

Verify that no foreign or deleterious material has been deposited within DG surfacing area.  Such materials include paint, paint washout, concrete slurry, concrete layers or chunks, cement, plaster, oils, gasoline, diesel fuel, paint thinner, turpentine, tar, roofing compound, acid.

If contamination by foreign or deleterious material or liquid is present within DG surfacing area, remove the contamination as directed by District Construction Manager and replace with new uncontaminated sub-grade materials.

Proceed with installation only after unsatisfactory conditions have been corrected.

PREPARATION

General: Proof-roll subgrade using heavy, pneumatic-tired rollers to locate areas that are unstable or that require further compaction.

INSTALLATION OF BASE AT STABILIZED DG SURFACING

Provide 3-inch deep compacted layer of specified base material.

Pre-soak base material with water and compact to 95% per ASTM D 1557.

Compaction testing to be performed by District testing agency prior to installation of stabilized DG surfacing.

INSTALLATION OF EDGINGS

Wood Edging:

Install wood edging at perimeter of surfacing except where DG surfacing abuts asphalt or concrete paving.

Anchor edging with wood stakes spaced 36 inches maximum apart, driven at least 1-inch below top elevation of edging.

Fasten edging to stakes with 2 galvanized nails per stake; nail length as necessary to penetrate both members and provide 1/2-inch clinch at point.

Predrill stakes if necessary to avoid splitting stakes.

INSTALLATION OF NON-STABILIZED DG SURFACING

Place and compact surfacing material at optimum moisture content to required grades, lines, cross sections, and thickness to not less than 95 percent of maximum dry unit weight according to ASTM D 1557.

Shape material to grades as indicated on Drawings.

Place materials in a single layer.

Compacted thickness shall be 4 inches minimum.

Compact surfacing with 5-ton or larger rollers or using other equipment acceptable to District Construction Manager.  Compact with vibratory-plate compactors in areas inaccessible to rollers.

INSTALLATION OF STABILIZED DG SURFACING

Binder manufacturer’s technical representative shall visit site at start of stabilized DG surfacing installation to verify installer understands correct installation methods.

Blending

For bidding purposes, mix at the rate of 15 pounds of binder per ton of aggregate.  Actual rate will be determined by binder manufacturer based on analysis of submitted aggregate sample.

Binder and aggregates must be dry during blending.

Thoroughly pre-mix binder into aggregate per manufacturer’s recommendations, including mixing apparatus.

Binder and aggregates must be dry during blending.

The following techniques are not acceptable:

Drop spreading binder over pre-placed aggregate.

Mixing by rototilling.

Bucket blending.

Placing

Do not place blended aggregate on filter fabric.

Place blended aggregate directly on prepared base.

Depth of blended aggregate: 4 inches minimum or as indicated on Drawings.

Place in equal thickness lifts not exceeding 3 inches per lift.  (For example, two 2-inch lifts for 4-inch total; two 2-1/2-inch lifts for 5-inch total, etc.)

Level to grades and cross-sections indicated on Drawings.

Watering

Water heavily for even, full-depth moisture penetration of blended aggregate.  Apply 25 to 45 gallons of water per ton of blended aggregate to achieve saturation.  Perform random moisture depth tests using manufacturer recommended probing device which reaches full depth.

If surface of aggregate dries significantly quicker than subsurface material, lightly mist surface before compaction.

Do not compact until stabilized aggregate is able to accept compaction from a 2-5-ton roller without separation, plowing or any other physical compromise of aggregate.  Obtain approval from Project Inspector.

Compaction

Complete compaction within 72 hours of after placing aggregate.  Do not begin compaction if pumping or pancaking of the surface occurs.

Perform compaction using 2-5-ton double drum roller, making 3-4 passes.  Do not use vibratory plate compactor or vibration feature on roller.

Compact stabilized aggregate to 90% relative compaction.

Carefully compact areas near planting and irrigation systems using 8-inch or 10-inch hand tamp.

Following compaction, lightly spray surface area with water.  Do not disturb surface with spray action.

INSTALLATION TOLERANCES

Thickness:  Compact to produce the thickness indicated within the following tolerances:

Surfacing Course:  Plus 1/4-inch, no minus.

Surface Smoothness:  Compact to produce a surface smoothness within the following tolerances as determined by using a 10-foot straightedge applied transversely or longitudinally to surfaced areas:

Surfacing Course:  1/4-inch (6 mm).

INSPECTION

General: Finished compacted surface shall be smooth and uniform, firm throughout profile, with no spongy areas.

Stabilized DG Surfacing: Finished surface shall have no evidence of chipping or cracking.  Loose material shall not be present on surface after installation.

Repair irregularities in surfacing to approval of District Construction Manager.

REPAIRS

Excavate damaged area to depth of aggregate and square off edgings or adjacent pavements.  If area is dry, moisten damaged portion lightly.

DG Surfacing: Install moisture conditioned aggregate matching existing material.  Install in excavated area to match finish grade and profile indicated on Drawings.

Stabilized DG Surfacing: Pre-blend matching aggregate and binder as recommended by binder manufacturer.  Add water to pre-blended material.  Thoroughly moisten mix with 25-45 gallons water per 1-ton of pre-blended material, or to approximately 10% moisture content.  Install moistened, pre-blended aggregate mixture in excavated area to match finish grade and profile indicated on Drawings.

Compact with an 8-inch or 10-inch hand tamp or 250-300 pound roller.

FIELD QUALITY CONTROL

Testing Agency:  District will engage a qualified testing agency to perform the following tests and inspections:

Compaction of base material at stabilized DG surfacing areas according to ASTM D 1557; one test per 1,000 square feet of base.

CLEANUP AND PROTECTION

Cleanup:  Promptly and carefully remove debris and excess excavated materials created by DG surfacing work.  Debris includes paper, grass clippings, organic material.  Remove by gentle mechanical blowing or hand raking.  Legally dispose of materials off District property.

Protection

Erect temporary fencing or barricades and warning signs as required to protect newly installed DG surfacing areas from traffic and public access.  Maintain fencing in place for 72 hours minimum after completion of installation.  Drying period might take longer due to weather conditions.

Do not permit vehicular traffic on finished surfacing.

Alert District Construction Manager to nearby landscape irrigation that could possibly create damaging conditions during and after installation.  Damaging conditions include standing water on or adjacent to surfacing.

MAINTENANCE SERVICE FOR STABILIZED DG SURFACING

Verify with District Project Manager that maintenance service is required for Project. Generally, maintenance period should align with plant maintenance periods.

Stabilized DG Surfacing Maintenance Service: Provide 180 day full maintenance by skilled employees of stabilized DG surfacing installer.

Coordinate start of stabilized DG surfacing maintenance period with start of landscape maintenance period to end at the same time.

END OF SECTION 32 15 40

Retain this notice in all Sections of Project Manual.

San Diego Unified School District Guide Specifications

Document Version: August 2021